## Slide 1
In-situ GIWAXS of thermally-induced co-crystallization in Doped Organic Semiconductor Films
6/09/2022
Alba Cazorla1, Adara Babuji1 , Eduardo Solano2, Carmen Ocal1*, Esther Barrena 1*
1 Institut de Ciència de Materials de Barcelona (ICMAB-CSIC)
2 ALBA Synchrotron

## Slide 2
ORGANIC SEMICONDUCTORS (OSCs)
Low-temperature processing
Low-cost production
Mechanical flexibility
Light weight
Applied to OLEDs, OFETs, solar cells, photodetectors..
[2] https://in-part.com/blog/top-nanotechnology-innovations-2017/
[1] https://www.eletimes.com/organic-semiconductors-for-flexible-electronic-devices
Organic Light Emitting Diodes
[1]
[2]
Possible issues:
Polymorphism
Needed microstructure control
Dewetting

## Slide 3
Gate
Dielectric
OSC film
Drain
Source
Organic Field Effect Transistors (OFETs)
[3] https://en.wikipedia.org/wiki/Organic_field-effect_transistor
[3]
High ordered crystalline structure  High charge carrier mobility
Challenging to have good charge injection from electrodes: MOLECULAR DOPING as a strategy
Structural characterization of the interface is key to understand charge transport properties

## Slide 4
MOLECULAR DOPING
Integer charge transfer (ICT)
Charge transfer complex (CTC)
LUMO
HOMO
OSC matrix
Binding Energy
LUMO
HOMO
OSC matrix
Binding Energy
p-dopant
CTC
p-dopant
CONVENTIONAL PICTURE
ALTERNATIVE MODEL
Improved device performance and control of the electrical properties of OSCs
(Mendez et al Angew. Chem. Int. Ed. 2013)
(Scaccabarozzi et al Angew. Chem. Rev. 2022)

## Slide 5
C8-BTBT-C8
DPh-BTBT
Mobility comparable or larger than polysilicon devices (1 cm2 V−1 s−1)
Highly ordered crystalline layers (lamellar structures)
Low-lying HOMO  air-stable devices
x Large contact resistance between source and semiconductor layer
Small molecule organic semiconductors: BTBT derivatives
[1]benzothieno[3,2-b][1]- benzothiophene
2,7 dioctyl -[1]benzothieno[3,2-b][1]- benzothiophene
2,7 diphenyl -[1]benzothieno[3,2-b][1]- benzothiophene
b
a
Herringbone arrangement
C8-BTBT-C8

## Slide 6
CmBTBT/FxTCNQ co-crystal reported
F6TCNNQ as p-type dopant
2 polymorphs reported
(Dasari et al. Adv. Funct. Matter. 2019)
LUMO
HOMO
F6TCNNQ
Binding Energy (eV)
BTBT derivatives
LUMO
HOMO
-5.43
(Mendez et al Angew. Chem. Int. Ed. 2013)
Intercalation
1:1 co-crystal structure for C10-BTBT-C10 : F4TCNQ
(co-deposited from solution)
α-polymorph
(trigonal system)
β-polymorph
(monoclinic system)
1,3,4,5,7,8-hexafluoro-tetracyanonapthoquinodimethane

## Slide 7
Thin Film growth
Thermal Evaporation
SiO2/Si(100)
OSC
Samples of this project were grown by Adara Babuji and Shunya Yan (PCSI group at ICMAB)
LINKAM heater stage
at NCD-SWEET Beamline (ALBA Synchrotron)
Structural characterization by Grazing-Incidence Wide-Angle X-ray Scattering (GIWAXS)
Evolution of the structure during thermal annealing
C8-BTBT-C8
DPh-BTBT
F6TCNNQ

## Slide 8
GIWAXS to understand thin film structure
Probed out-of-plane (OOP) and in-plane (IP) scattering:
Structure
Crystallinity degree
Crystallite orientation
Possible to get information about:
2D detector
In-plane (IP) ∼
OOP

## Slide 9
Same structure as the reported one
Remarkable shift of the in-plane peaks to lower q values
Film partially desorbed at 110 °C
29.0 Å
b
At 25 °C
At 100 °C
a
b (+4 %)
< 1 %
IP
OOP
IP
Thermal expansion
Line cuts
2D GIWAXS patterns
a (Å) | b (Å) | c (Å) | α (°) | β (°) | γ (°)
5.90 | 7.97 | 28.7 | 90 | 92.44 | 90
C8-BTBT-C8 (20nm)
(Space group: P/c)

## Slide 10
At RT, three structures coexist: C8-BTBT-C8 + F6TCNNQ + co-crystal
EFFECT OF ADDING THE MOLECULAR DOPANT
‘Charge Transfer Complexes in Organic Field-Effect Transistors: Superior Suitability of Surface Doping’,
A. Babuji, A.Cazorla, E. Solano, C. Habenicht, C. Ocal, K. Leo, E. Barrena (Submitted May 2022).
OOP Line cuts
(001)
(001)c
(011)
(111)
F6TCNNQ (14nm) on C8-BTBT-C8 (20nm)
Co-crystal peak observed at (spacing of 19 Å) corresponding to (001)c plane

## Slide 11
EFFECT OF POST-ANNEALING AFTER ADDING THE MOLECULAR DOPANT
Annealing promote co-crystal formation.
Co-crystals have higher thermal stability than the pristine BTBT films.
‘Charge Transfer Complexes in Organic Field-Effect Transistors: Superior Suitability of Surface Doping’,
A. Babuji, A.Cazorla, E. Solano, C. Habenicht, C. Ocal, K. Leo, E. Barrena (Submitted May 2022).
OOP Line cuts
F6TCNNQ (14nm) on C8-BTBT-C8 (20nm)

## Slide 12
IP
(110)
(020)
(120)
(200)c
Co-crystal peaks are observed at (spacing of 19 Å) 1.86(spacing of 3.4 Å) and at 0.79 (spacing of 7.9 Å) corresponding to (001)c, (200) and (010) co-crystal planes
25 °C (final)
130 °C
(001)c
(01L)c
(20L)c
(01L)c
(20L)c
Co-crystal
C8-BTBT-C8
a
b
29 Å
(200)c
(010)c
(001)c
F6TCNNQ (14nm) on C8-BTBT-C8 (20nm)

## Slide 13
(11L)
(12L)
(001)
(02L)
(002)
(003)
DPh-BTBT thin film 25 °C
Same crystal structure as the reported one
NO thermal expansion
Effect of temperature in the structure of the film
IP
Line cuts
OOP
19.3 Å
b
a
IP
OOP
BTBT core
a (Å) | b (Å) | c (Å) | α (°) | β (°) | γ (°)
6.20 | 7.85 | 19.3 | 90 | 93.06 | 90
(Space group: P/c)
DPh-BTBT (20nm)

## Slide 14
No co-crystal formation
EFFECT OF POST-ANNEALING AFTER ADDING THE MOLECULAR DOPANT
F6TCNNQ (14nm) on DPh-BTBT (20nm)

## Slide 15
Conclusions
Side groups play a role on thermal expansion
Co-crystal structure formed for F6TCNNQ deposited on C8-BTBT-C8, promoted with annealing
Thermal expansion of the in-plane unit cell facilitates the formation of co-crystal.
Co-crystalline structure has a higher thermal stability than the pristine film
Substrate
C8 BTBTC8
F6TCNNQ
Substrate
C8 BTBTC8
Dopant Deposition
Substrate
Annealing
(up to 130 °C)
Substrate
DPhBTBT
F6TCNNQ
Substrate
DPhBTBT
Stable structure
F6TCNNQ
Dopant Deposition
Annealing
F6TCNNQ
Substrate
DPhBTBT

## Slide 16
THANK YOU ALL
The PCSI Research Group:
Prof. Carmen Ocal
Dr. Esther Barrena
Adara Babuji
Shunya Yan
Shaghayegh Mesforoush
ALBA:
Dr. Eduardo Solano
(NCD-SWEET Beamline)

## Slide 18
EXTRA SLIDES

## Slide 19
MISSING WEDGE USING GIWAXS
http://gisaxs.com/index.php/GI_missing_wedge
qz obtained from GIWAXS experiments is NOT a true specular scan
2D GIWAXS patterns: 2D slices through the 3D-reciprocal space

## Slide 20
DATA CONVERSION FROM PIXELS TO RECIPROCAL MAP
Raw (pixels)
Converted
Data treatment with python package (pyFAI)
Emergence of missing data along qz=0 in the reciprocal space

## Slide 21
Data Analysis
Out-of-plane (OOP)
In-plane (IP)
-90°
χ
0°
Missing wedge
OOP
OOP
IP
IP
GIXD Data treatment with pyFAI
Detector image in pixels
Experimental geometry parameters
Conversion to q-space
Calibration (Cr2O3 as ref. material)
(Ashiotis et al J. App. Crystallography, 2015)

## Slide 22
25 °C
80 °C
100 °C
110 °C
120 °C
130 °C
25 °C (final)
(11L)
(12L)
(001)c
(001)
(02L)
(01L)c
F6TCNNQ/C8-BTBT-C8 sample for an incident angle of 0.12 °
Notes: A2. 2D GIXD maps of F6TCNNQ/C8BTBT sample acquired at different temperatures for an incident angle of 0.12º.

## Slide 23
25 °C
(11L)
(12L)
(001)
(02L)
100 °C
110 °C
120 °C
150 °C
160 °C
25 °C (final)
F6TCNNQ/DPh-BTBT sample for an incident angle of 0.12 °
Notes: A4. 2D GIXD maps of F6TCNNQ/DphBTBT sample acquired at different temperatures for an incident angle of 0.12º.

## Slide 24
Multiple peak effect
Peak splitting appears for incident (αi) and scattering (αf ) angles close to the critical angle of the substrate because of 2 different scattering pathways of the incident X-rays:
Direct Bragg scattering at the organic crystallites
An optically reflected primary beam at the substrate and subsequent Bragg scattering at the organic layer

## Slide 25
BTBT derivatives: Crystal Structure
Herringbone arrangement
c
b
a
(001) plane
α
γ
β
c
a
b
a
Lamella structure
C8-BTBT-C8
Same crystal symmetry for Dph-BTBT (for bulk or thin films form)