## Slide 1: Application of synchrotron-based techniques for the study of calcium oxalate hydrates transformation
a GTS Research Group, Department of Chemistry, Faculty of Science, Universitat Autònoma de Barcelona, 08193 Bellaterra, Cerdanyola del Vallès, Spain.
b ALBA Synchrotorn Light Source, Cerdanyola del Vallès, Barcelona, Spain
Iris H.Validoa, Roberto Boadaa, Montserrat Resina-Gallegoa, Victor Fuentes-Cebriána, Ibraheem Yousefb, Oriol Vallcorbab, Manuel Valientea, Montserrat López-Mesasa

## Slide 2
PRESENTATION INDEX
1. Introduction
2. Objectives
3. CaOx characterization
4. Organic matter distribution
5. COM formation origin
6. Conclusions

## Slide 3
1. INTRODUCTION

## Slide 4
1. INTRODUCTION
Kidney Stones vs. Giving Birth
WHAT IS MORE PAINFUL?
©DreamWorks Animation
Solid concretion in the urinary tract
Incapacitating pain
©Giphy.com
©Giphy.com

## Slide 5
1. INTRODUCTION – Epidemiology and cost for the health care system
7-15%
3-6%
30-50% in 5 to 10 years
75% after 20 years
©Giphy.com

## Slide 6
1. INTRODUCTION – Formation hypotheses
Urinary saturation
Crystal germination
and growth
Crystal aggregation
and agglomeration
Retention of
crystallized particles

## Slide 7
1. INTRODUCTION – Formation hypotheses
STONE
Calcium
Oxalate
Sodium
Urate
Cystine
Organic matter
Citrate
Pyrophosphate
Phytate
Mg
Organic matter
Promoters
Inhibitors

## Slide 8
1. INTRODUCTION – Kidney stone classification
Infrared spectroscopy
X-ray diffraction
Chemical analysis
Bulk analysis
Morpho-constitutional analysis

## Slide 9
1. INTRODUCTION – Kidney stone classification
Kidney Stones
Oxalate
Phosphate
Uric Acid
Cystine
Others
Calcium Oxalate (CaOx)
Dihydrate (COD)
Monohydrate (COM)
Calcium Phosphate (CaP)
Struvite (STR)
Hydroxyapatite (HAP)
Brushite (BRU)
Anhydre (AUA)
Dihydrate (AUD)
Mixed

## Slide 10
1. INTRODUCTION – Kidney stone classification
TRANSFORMATION
(Lost of one molecule of water)
Dihydrated
(Kinetically favorable)
(Thermodynamically stable)
Contact time with the solution (urine)
Deficit of stabilizers
COD
TRA
COM
=
=
X
?
CaC2O4·H2O
CaC2O4·2H2O
Monohydrated
Origin
Different pathologies
Hyperoxaluria
Hypercalciuria

## Slide 11
2. OBJECTIVES

## Slide 12
2. OBJECTIVES
COD
TRA
COM
Crystalline conversion
?
Origin
Crystalline conversion
COM vs. TRA
Formation origin?
Organic matter
Promoters or inhibitors?
COD stabilization

## Slide 13
3. CaOx
CHARACTERIZATION

## Slide 14
3. CaOx CHARACTERIZATION – Experimental section
Characterization
X-ray Diffraction (XRD)
X-ray Absorption Spectroscopy (XAS)
©2014 CELLS
X-ray absorption near edge structure (XANES)
Extended X-ray absorption fine structure (EXAFS)
(Local site symmetry, charge state, orbital occupancy)
(Local structure (bond distance, number, type of neighbors…))
Infrared spectroscopy
Vibrational spectroscopy characterization
Theoretical frequencies calculated via DFT with Gaussian software
Notes: For the characterization of the synthetized crystals, four different techniques were used:

## Slide 15
3. CaOx CHARACTERIZATION – Results and discussion
XRD
XAS
Oxalate ion coordination
P21/c
I4/m
COM
COD

## Slide 16
3. CaOx CHARACTERIZATION – Results and discussion
COM
COD
Infrared spectroscopy (IR)

## Slide 17
3. CaOx CHARACTERIZATION – Results and discussion

## Slide 18
4. ORGANIC MATTER
DISTRIBUTION
Notes: This section corresponds to the second article, Calcium oxalate kidney stones, where is the organic matter? A synchrotron based infrared microspectroscopy study, already published in the journal of Biophotonics.

## Slide 19
4. ORGANIC MATTER DISTRIBUTION – Experimental section
SR-µIR in transmission mode
Resolution: 4 cm-1
Apperture size: 10x10 µm2
Nº of scans: 512

## Slide 20
4. ORGANIC MATTER DISTRIBUTION – Results and discussion
Organic matter distribution
* Bunaciu, A. A., et. al., Appl Spectros Rev, 2015, 50:176-191
*
CH2 asym. Stret.
(~2920 cm-1)
CH3 asym. Stret.
(~2960 cm-1)
Lipids
Proteins

## Slide 21
4. ORGANIC MATTER DISTRIBUTION – Results and discussion
Organic matter distribution
Lipids
Proteins
COD
COM
Surface
Nucleus

## Slide 22
5. COM
FORMATION ORIGIN
Notes: This section corresponds to the third article, Discriminating the formation origin of calcium oxalate monohydrate in kidney stones via synchrotron microdiffraction.

## Slide 23
5. COM FORMATION ORIGIN – Experimental section
COM
COD
TRA
30 µm thickness
EpoFix resin
Beam size: 15 µm2
MSPD beamline
µXRD
Resolution: 4 cm-1
Apperture size: 12x12 µm2
Nº of scans: 128
SMIS beamline
µIR

## Slide 24
5. COM FORMATION ORIGIN – Results and discussion
SR-µIR in reflectance mode

## Slide 25
5. COM FORMATION ORIGIN – Results and discussion
SR-µXRD

## Slide 26
5. COM FORMATION ORIGIN – Results and discussion
2D µXRD patterns
COM
COD
0
360
φ (º)
180º
TRA

## Slide 27
5. COM FORMATION ORIGIN – Results and discussion
TRA (S26A)
COM (S23)
HAP

## Slide 28
5. COM FORMATION ORIGIN – Results and discussion
(100)
(040)
COM (S23)
TRA (S26A)

## Slide 29
5. COM FORMATION ORIGIN – Results and discussion

## Slide 30
5. COM FORMATION ORIGIN – Results and discussion
(100)
(040)
??? (S33)
COM
COM
TRA

## Slide 31
6. CONCLUSIONS

## Slide 32
6. CONCLUSIONS
Characterization of calcium oxalate hydrates
The long-range (XRD) and short-range (XAS) order characterization of the synthetic oxalocalcic species , in combination with the application of DFT computational analysis, allowed to assign the characteristic bands from the infrared spectra to the corresponding vibration.
Proteins could act as promotors of the COM formation since they are found in the nucleus.
Distribution of the organic matter on oxalocalcic stones
It was possible to determine that lipids participate in the stabilization of COD crystallites and as possible inhibitors of the COM formation/development.
By analyzing the asymmetric stretching of the aliphatic –CH2- and –CH3 on the SR-µFTIR study, it was possible to differentiate between proteins and lipids.
Formation origin of calcium oxalate monohydrate
Due to the high variability on the oxalocalcic spectra by applying SR-µFTIR in reflectance mode, the differences observed between COM and TRA are not considered significant enough to distinguish them with this technique.
However, it is possible to distinguish them by studying their crystalline texture degree with the qualitative analysis of the azimuthal plot of the selected reflections from the 2D µ-XRD data.

## Slide 33
ACKNOWLEDGEMENTS

## Slide 34
ACKNOWLEDGEMENTS

## Slide 35
Thanks for your attention!
©Giphy.com

## Slide 36: Application of synchrotron-based techniques for the study of calcium oxalate hydrates transformation
a GTS Research Group, Department of Chemistry, Faculty of Science, Universitat Autònoma de Barcelona, 08193 Bellaterra, Cerdanyola del Vallès, Spain.
b ALBA Synchrotorn Light Source, Cerdanyola del Vallès, Barcelona, Spain
Iris H.Validoa, Roberto Boadaa, Montserrat Resina-Gallegoa, Victor Fuentes-Cebriána, Ibraheem Yousefb, Oriol Vallcorbab, Manuel Valientea, Montserrat López-Mesasa

## Slide 37
Urinary tract
Kidney section
Neprhon
Support

## Slide 38
Organic matter distribution
*
* Mallamace, F., et. al., Comput Struct Biotechnol, 2014, 13:33-7
** Bunaciu, A. A., et. al., Appl Spectros Rev, 2015, 50:176-191
**
CH2 asym. Stret.
(~2920 cm-1)
CH3 asym. Stret.
(~2960 cm-1)
Support

## Slide 39
Support

## Slide 40
Support

## Slide 41
Support

## Slide 42
Support

## Slide 44
Support

## Slide 45
Support

## Slide 46
Support
(100)
(040)

## Slide 47
Support