## Slide 1
Rashba-like spin textures in Graphene promoted by ferromagnet-mediated Electronic-Hybridization with heavy metal.
Beatriz Muñiz Cano, A. Gudín, A Anadón, J. M. Díez, P. Olleros-Rodríguez, Fernando Ajejas,
I. Arnay, M. Jugovac, J. Rault, P. Le Fèvre, F. Bertran, D. Mazhjoo, G. Bihlmayer, S. Blügel, R. Miranda, J. Camarero, Miguel Angel Valbuena, Paolo Perna.
X AUSE Conference & V ALBA user’s meeting.
Alba synchrotron, Barcelona 5-8 september 2022

## Slide 2
Introduction:
  SOC in graphene.
  Engineering Gr/FM/HM/oxide insulators Heterostructures for spintronics
ARPES Gr/Ir(111)/Al2O3(0001)
Conclusions
Outline
Intercalating Co:
  Gr/2 ML Co/Ir(111): ARPES, Spin-ARPES, DFT calculations
  Gr/10 ML Co/Ir(111)

## Slide 3
Emergent phenomena induced by spin-orbit coupling (SOC) at surfaces and interfaces:
- Social needs of developing new devices faster, more efficient, cleaner and that require less energetic consumption:
A. Soumyanarayanan,et al. Nature 539 (2016) 509
Introduction: Spin-Orbit Coupling Phenomena
Spin-Charge conversion (FM/NM) heterostructures (Edelstein effect).
Non-volatile MRAM SOT devices
Rashba states, topological states…
DM Interaction -> skyrmions, domain chiral wall
SOC in 2D materials at the basis of high speed, low energy consumption devices
Graphene based heterostructures for spintronics?

## Slide 4
Why Graphene ?
Long spin diffusion length
Long spin lifetime
But … negligible SOC !
Spintronics, Spin-Orbitronics devices
Induce SOC in gr by heavy metal intercalation, gating, functionalization, …
Introduction: Inducing a giant Spin-Orbit Coupling in graphene
hν=21.2 eV
Spin-split Graphene bands by a Giant
Spin Orbit interaction induced by Pb atoms
F. Calleja et al. Nat. Phys. (2015) 11, 43
M. Garnica, et al. Nat. Phys. (2013) 9, 368
D. Maccariello et al. Chem. Mat. (2014) 26, 2883
Gr/Pb/Ir(111)
Pb-intercalated Gr / Ir(111) by STM
Otrokov et al. 2D Mater. 5 (2018) 035029
SR-ARPES
Yang, H., Chshiev, M. et al. Nature materials, 17(7), 605. 2018
Significant DMI at graphene–ferromagnet interfaces due to the Rashba effect
Notes: Graphene presents very interesting properties for spintronics, since it is an optimal spin conductor due to its long spin difussion length and spin lifetime. To design spintronic devices we need also to convert and measure spin currents and that is usually done taking advantage of the Spin Hall effect or other SOC induce effects. Graphene by itself does not present SOC, but it has been reported that the intercalation of appropiate elements can induce Rashba type SOC.
SOC SPARPES our group

## Slide 5
Spin-orbitronics group at IMDEA (P. Perna):
Engeneering Gr/FM/HM heterostructures on insulating oxides.
Choose of the suitable oxide substrate: MgO(111), STO(111), Al2O3(0001)
Sputtered HM (Ir, Pt) epitaxial buffers on insulating crystals @ 500 ºC
In-situ UHV CVD gr growth @ 750 ºC
Co RT Evaporation & Intercalation of Co @ (595-665 K)
Monitoring by XPS and LEED, STM at each stage
Avoiding Co/HM intermixing (checked by XPS)
Growth of fully epitaxial graphene/FM/HM interfaces on oxide substrates
Direct implementation on devices, induced or generated electrical/spin currents not drained by metallic syngle crystals
Missing electronic band structure characterization
Elucidate electronic origin of Rashba SOC in the interface
UHV epitaxial growth process:
Ajejas, et al. ACS Appl. Mater. Interfaces 2020, 12, 4088−4096
70 eV
Ajejas et al. Nano Lett. 2018, 18, 5364
Pt
Co
ML graphene
DMI
DMI
n-doped
Unexpected giant Rashba-like DMI at gr/Co OPPOSITE to SOC-induced Co/Pt

## Slide 6
Preprint at B. Muñiz Cano, A. Gudín, Al. Anadón,…, M. A. Valbuena, P. Perna arXiv:2206.04351 [cond-mat.mtrl-sci]
Electronic structure epitaxial graphene/Ir(111) on oxide insulating substrates
Fermi Surface and Constant: Trigonal Dirac cone
Weak Interacting Gr electronic band structure
n-doped preserved Dirac cone
ARPES electronic band comparable to
Gr monolayer grown on Ir(111) single crystals
ARPES on Gr/Ir(111)/Al2O3(0001)
Samples grown at MBE chamber (IMDEA) and transferred in UHV to Cassiopée Beamline (Soleil Synchrotron)

## Slide 7
Electronic structure vs thickness intercalated Co
Co intercalation
2 ML Co
10 ML Co
Gr/Ir(111)/
Al2O3(0001)
Weakly interacting Gr
Gr  and 
Ir(111) FS features
Rashba SS state
Strong charge transfer.
Shift  2eV Gr .
Dirac cone Apex  2eV
Intense and well-defined Co 3d states
Splitting Gr  band:
Non interacting Gr
Interacting Gr
Co localized states
Highly quality epitaxial thin films
Is there any interaction Gr, Co, Ir states?
Preprint at B. Muñiz Cano, A. Gudín, Al. Anadón,…, M. A. Valbuena, P. Perna arXiv:2206.04351 [cond-mat.mtrl-sci]
Notes: Co

## Slide 8
Electronic structure vs 2 ML Co intercalated:
Interaction Co 3d and Ir states
2 ML Co
Gr/Ir(111)/
Al2O3(0001)
Ir Rashba SS
Ir 5d FS states
Co 3d states
hybridization between Co 3d states and Ir 5d states close to M point.
Hybridization between Co 3d states and Ir Rashba SS
ARPES band maps
Interaction between Ir states and Co states can induce giant SOC at the interface
Preprint at B. Muñiz Cano, A. Gudín, Al. Anadón,…, M. A. Valbuena, P. Perna arXiv:2206.04351 [cond-mat.mtrl-sci]
Blanco-Rey et al. Phys. Rev B 106, 064426 (2022)
Consistent with recent DFT calculations where Gr/Co and Co/HM interfaces have similar contributions from the strongly hybridized SOC-split d bands
Gr-capped 3d/5d metal heterostructures richer physics than what is expected from the prediction of single-band models, such as the Rashba DMI model.

## Slide 9
Electronic structure vs 2 ML Co intercalated:
Interaction Co 3d and Ir states
2 ML Co
Gr/Ir(111)/
Al2O3(0001)
ARPES Fermi Surface and Constant Energy maps
Ir FS elipsoidal pockets preserved after intercalation
Co 3d hybridization wih Ir  closer elipsoidal pockets
Interaction between Ir states and Co states can induce giant SOC at the interface
Prominent state ak K ?
Preprint at B. Muñiz Cano, A. Gudín, Al. Anadón,…, M. A. Valbuena, P. Perna arXiv:2206.04351 [cond-mat.mtrl-sci]

## Slide 10
Electronic structure vs 2 ML Co intercalated:
Interaction Co 3d and C states
2 ML Co
Prominent state ak K ?
Hybridization C 2p – Co 3d
Preprint at B. Muñiz Cano, A. Gudín, Al. Anadón,…, M. A. Valbuena, P. Perna arXiv:2206.04351 [cond-mat.mtrl-sci]
Mini Dirac Cone Fully spin polarized.
Usachov et al. Nano Lett. 2015, 15, 2396−2401
Previously reported for Gr/Co(0001) single crystal.
Mini Dirac Cone at K at EF. Bandwidth  200 meV
Fully spin polarized Mini Dirac cone developed on thin film samples grown onto insulating substrates
Spintronic devices

## Slide 11
In-plane spin texture of graphene π-bands in the presence of Rashba SOC
Nano Lett. 2018, 18, 1564−1574
Spin Resolved ARPES measurements:
Energy Spin Splitting and Spin Polarization
E  100 ± 40 meV
E  20 ± 40 meV
uct
Out-of-Plane
In-Plane
Out-of-Plane
In-Plane
In-plane energy splitting and spin polarization of the same order of others Rashba-SOC systems (Pb, Au intercalated…)
Negligible out-of-plane energy splitting and spin polarization
Zoom Gr  Peak
Co 2 ML
2 ML Co
Preprint at B. Muñiz Cano, A. Gudín, Al. Anadón,…, M. A. Valbuena, P. Perna arXiv:2206.04351 [cond-mat.mtrl-sci]

## Slide 12
Spin Polarized Electronic Structure Gr/2 ML Co/Ir(111)
DFT calculations
E 100 meV
In-plane spin Sy
Fully spin polarized mini Dirac Cone (Co-C interaction)
Hybridization Co/Ir states (EF - 3eV)
In-plane energy spin splitting (Gr  -6, -4 eV)
DFT calculations largely agree with experimental ARPES and SR-ARPES results
Neglect charge transfer effects
2 ML Co
Preprint at B. Muñiz Cano, A. Gudín, Al. Anadón,…, M. A. Valbuena, P. Perna arXiv:2206.04351 [cond-mat.mtrl-sci]

## Slide 13
10 ML Co
Negligible In-plane and out-of-plane energy spin splitting
Thicker Co layer decouples Gr from SOC Ir source
Spin Polarized Electronic Structure Gr/10 ML Co/Ir(111)
Consistent with recent DFT calculations where Gr is decoupled for more than 3 FM ML
Blanco-Rey et al. Phys. Rev B 106, 064426 (2022)
Preprint at B. Muñiz Cano, A. Gudín, Al. Anadón,…, M. A. Valbuena, P. Perna arXiv:2206.04351 [cond-mat.mtrl-sci]

## Slide 14
CONCLUSIONS
Gr/2 ML Co/Ir(111)/Al2O3(0001):
  Identify SOC source from Ir-Co-C hybridization.
  We resolve fully spin polarized mini Dirac cone (as from Gr grown on Co(0001) single crystal)
  Rashba-like spin texture determined fron SR-ARPES and DFT calculations
  Consistent with recent DFT predictions where not only a Rashba like scenario should be considered at the DMI of Gr/Co.interface
Gr/10 ML Co/Ir(111)/Al2O3(0001)
  Increasing Co thickness decouples Gr from SOC induction
Gr/Ir(111)/Al2O3(0001) Weak interacting Gr electronic band structure. Dirac cone preserved. Slightly n-doped. Similar to Gr grown on Ir(111) single crystals
We have determined the electronic structure of Gr onto Ferromagnetic / Heavy Metal interfaces grown onto oxide insulating surfaces, suitable to be implemented in electronic/spintronic devices

## Slide 15
Financial Support:
Spin-ARPES: EQC2019-006304-P
SpOrQuMat: PGC2018-098613-B-C21
SOnanoBrain PID2020-116181RB-C31
CONPHASETM PID2021-123776NB-C21
Programa Operativo de Empleo Juvenil y la Iniciativa de Empleo Juvenil.
Consejeria Ciencia, Universidades e Innovación PEJD-2019-PRE/IND-17048
Project P2018/NMT-4321 (NANOMAGCOST-CM).
Programme for Centres of Excellence in R&D
Grant: SEV-2017-0706
Spin-ARPES
B. Muñiz Cano.
M. A. Valbuena
Spin-Orbitronics
A. Gudín A. Anadón
J. M. Diaz F. Ajejas
I. Arnay P. Olleros
P. Perna
J. Camarero
R. Miranda
Synchrotron experiments
J. Rault, P. Le Fèvre, F. Bertran
M. Jugovac
Acknowledgments:
DFT Calculations
D. Mazhjoo, G. Bihlmayer, S. Blügel

## Slide 17
Pt
Co
n-doped graphene
Origin of the unusual (large) DMI at gr/Co
SOC-DMI at Co/Pt interface
Three-sites model (Fert-Levy) based on HM impurities in Co layer
Rashba-like DMI at gr/Co (existence of sizeable electric field)
F. Ajejas, AA, PP et al. Nano Lett. 2018, 18, 5364
Fert A. & Levy P. M., Role of Anisotropic Exchange Interactions in Determining the Properties of Spin-Glasses, Phys. Rev. Lett. 44, 1538–1541 (1980).
Kundu A et al. Phys. Rev. B 92, 094434 (2015)
F. Ajejas, PP et al. Nano Lett. 2018, 18, 5364
Yang, H., et al. Nature materials, 17(7), 605.
Rashba-like DMI at gr/Co OPPOSITE to SOC-induced Co/Pt
Notes: conduction electron mediated Rashba−DMI mechanism