## Slide 1
Recent Progress on Synchrotron Radiation Based Operando Characterization of Battery Materials at Alba Synchrotron
Ashley P. Black,a Giovanni Agostini, b Carlos Escudero, b François Fauth, b Carlo Marini, b M. Rosa Palacin, a Alexandre Ponrouch, a Laura Simonelli, b Andrea Sorrentino,b Dino Tonti, Ibraheem Yousef b
a Institut de Ciència de Materials de Barcelona (ICMAB-CSIC)
b CELLS - ALBA synchrotron
ablack@icmab.es
PTI+ TRANS-ENER+
Transición Energética Sostenible

## Slide 2
Next generation Li Battery and beyond…
Decarbonization, net zero GHG by 2050… <+1.5°C …
Transportation
Grid scale electric storage
Personal electronics
NMC/Li rich
All Solid State
Li Metal
Alternative Anodes, Si,…
Li/S, Li/Air
Na-ion, Na/S, K/S,…
Multivalents, Mg, Ca, Al
Aq. Zn/MnO2
Organic Battery
100TWh
600GWh
(Global Capacity)
20GWh
100% Renewable by 2050 (100 TWh) 95 gigafactories +125 (80M cars/year)
1.2TWh (2030)
$10-20/kWh
10% CAGR (compound annual growth rates) sustained for 30 years
Prof. Yet-Ming Chiang, MIT (https://energy.mit.edu) Future of Energy Storage

## Slide 3
Synchrotron radiation:
Nondestructive analytical techniques
Probing electronic and geometric structures at various length and time scales
Spectroscopy, scattering, and imaging
Ex-situ, in-situ or Operando
Synchrotron radiation based operando characterization of battery materials
F. Lin et al. Chem. Rev. 2017, 117, 13123.

## Slide 4
Compatible with experimental set up but electrochemically efficient
O. J. Borkiewicz et al., J. Appl. Cryst., 45, 1261 (2012), R.E. Johnsen et al., J. Appl. Cryst., 46, 1537 (2013),Ravnsbaek et al., Nano Letters (2014)
Electrochemical Cell for Operando Studies of Batteries Using Synchrotron Radiation

## Slide 5
Operando capabilities at Alba Synchrotron
Operando at

## Slide 6
Operando at MSPD (Powder Diffraction beamline)
Operando Leriche type cells
Thermalized cells
Glass and Kapton coin cells
Michael Knapp, Helmut Ehrenberg (KIT)
Technical Specifications | 
Energy range | 8 - 50 keV
Flux | ~ 4·1012 ph/s
Energy resolution | 2·10-4
Black, A. P. et al. ENERGY STORAGE MATER. Vol.47,2022,354-364. (2022)
LRCS

## Slide 7
Operando capabilities at Alba Synchrotron
Operando at

## Slide 8
Operando at CLÆSS: the X-ray absorption and emission spectroscopy beamline
1
2
Can Wu et al., Adv. Mater. 2022, 2108363
Operando conditions accessible at CLÆSS down to the S K-edge
Technical Specifications | 
Energy range XAS | 2.4 – 63.2 KeV
Energy range XES | 6-22 KeV
Acquisition mode | TR, TFY, PFY, TEY
Spot size | between 200x100 µm2 and 8x1 mm (HxV)

## Slide 9
Operando at CLÆSS: the X-ray absorption and emission spectroscopy beamline
Aqueous Zn-MnO2 batteries
Wenhai Wanga, Cheng Liua, Ashley P. Blacka, Vlad Martin-Diaconescub, Laura Simonellib, Anna Laromaine,a Anna Roig,a Dino Tonti a
2 M ZnSO4 with 0.2 M MnSO4 aqueous electrolyte
Formation of Zn4(OH)6SO4·5H2O

## Slide 10
Operando at CLÆSS: the X-ray absorption and emission spectroscopy beamline

## Slide 11
Fast Data Analyzer (FDA)
Operando Software development
Operando Ploter (Oplot)
Available at MSPD and NOTOS
Available at CLAESS and NOTOS
Carlo Marini
Carlos Frontera

## Slide 12
Operando capabilities at Alba Synchrotron
Operando at

## Slide 13
Operando PD+XAS at NOTOS
Technical Specifications | 
Monochromator | DCM (Si 111 and Si 220)
Energy range | 4.9 to 30 keV (<Ti K-Edge)
Flux | 1011 ph/s
Spot size | between 100 µm2 and 3x1 mm (HxV)
Operando Cells Leriche type and 2032 CoinCells

## Slide 14
Operando PD+XAS at NOTOS
• Lithium Nickel Manganese Cobalt Oxide (NMC111)
Active Material Loading: 12.9 mg/cm2 ± 5%
Capacity: ≥ 170 mAh/g (2.5 – 4.1V @0.1C)
• Lithium Iron Phosphate (LiFePO4)
Active Material Loading: 7.3 mg/cm2 ± 5%
Capacity: ≥ 155 mAh/g (2.7 – 4.3V @ 0.1C)
Cycled vs Li metal (MTI disc) in LP30 electrolyte ( LiPF6 in EC:DMC)

## Slide 15
Operando PD+XAS at NOTOS
• Lithium Nickel Manganese Cobalt Oxide (NMC111)
Active Material Loading: 12.9 mg/cm2 ± 5%
Capacity: ≥ 170 mAh/g (2.5 – 4.1V @0.1C)
• Lithium Iron Phosphate (LiFePO4)
Active Material Loading: 7.3 mg/cm2 ± 5%
Capacity: ≥ 155 mAh/g (2.7 – 4.3V @ 0.1C)
Cycled vs Li metal (MTI disc) in LP30 electrolyte ( LiPF6 in EC:DMC)
Point A PD (1min) 11KeV
Point B PD+XAS (318s) Ni K-edge
Beam Inhibition, reversible, independent of cell geometry, time and energy dependent

## Slide 16
EXAFS
70%
EXAFS
90%
XANES
70%
XANES
90%
Operando PD+XAS at NOTOS
B(1min PD + EXAFS Ni (3min))
B(1min PD + XANES Ni (68s))
A(1minPD+1min Rest)
A(1minPD+1min Rest)
At1= 70% (100um Al) vs At2= 90% (250um Al)

## Slide 17
At1 70% A(1minPD+1min Rest) + B(1min PD + EXAFS Ni (3min))
Operando PD+XAS at NOTOS
At2 90% A(1minPD+1min Rest) + B(1min PD + EXAFS Ni (3min))

## Slide 18
Operando PD+XAS at NOTOS
Beam induced inhibition mechanisms
Gasification of the electrolyte dyes out the electrolyte at the measurement spot preventing from electrochemical reaction to occur
Ar (g), CO2 from electrolyte decomposition
Main Factors
- Photon Energy (Near edge)
- Photon Flux
- Exposure Time/Rest Time
- Number of Points (2-3)
- Spot size (Focus)
• Porosity
• Stack pressure/rigidity
• Electrode wettability
• Electrolyte/electrode ratio
• Electrolyte viscosity and volatility
• Particle size ( nano, micro, meso)
• Stability (Structural, thermal, electrochemical)
• Composition and Solubility

## Slide 19
Operando capabilities at Alba Synchrotron
Operando at MIRAS

## Slide 20
Operando at MIRAS
Operando infrared microspectroscopy in battery application: Lithium, sodium and calcium reversible intercalation in polyimide homopolymer (PIHOMO) and co-polymer (PI-COPO) positive electrode materials.
Technical Specifications | 
Source | Bending magnet, edge + constant field
Energy range | 1.2 to 100 µm (Far and middle IR)
Flux | Aprox. 4e+13 Ph/s
Spot size | 10x10µm2
Operando Cell (ECC-Opto-Std, EL CELL)

## Slide 21
Operando at MIRAS
Polyimide as Cathodes for Alkali- (Li+, Na+) and Alkaline Earth (Ca2+, Mg2+)-Metal-Ion Organic Batteries
1M LiTFSI
1M NaTFSI
0.5M Mg(TFSI)2
0.5M Ca(TFSI)2
1703
1673
1580
1455
1355
1255
1175
1100
Stretching ternary amide
Ring and CH Stretching
Skeletal vibration
(C)3-N Streching
C-N Streching
Infrared Spectra (FTIR) of the Polyimide Cathodes

## Slide 22
Operando at MIRAS
Sample Sample+CaF2
Sample+Sapphire
Sample+Glass
200µm SrF2
500µm ZnSe
500µm Si
Interference pattern due to partial reflection
Feynman, Richard (1985). QED: The strange theory of light and matter. Princeton University Press. ISBN 0-691-08388-6.

## Slide 23
Synchrotron Source
Globar Source
Operando at MIRAS
Spatial and Temporal Resolution of Synchrotron Radiation vs Internal Source
Polyimide/LiTFSI in DG /ACC
with ECC-Opto-ELCELL and Si (500µm)

## Slide 24
Operando FTIR at MIRAS

## Slide 25
Operando FTIR at MIRAS
Polyimide/1M LiTFSI in DG /ACC with ECC-Opto-ELCELL and Si (500µm)

## Slide 26
Operando FTIR at MIRAS

## Slide 27
Operando FTIR at MIRAS
Fast Operando Infrared Microspectroscopy Maping (5C)

## Slide 28
Operando capabilities at Alba Synchrotron
Steps towards In-situ Microscopy at

## Slide 29
Steps towards In-situ Microscopy at MISTRAL SOFT X-RAY MICROSCOPY BEAMLINE
Technical Specifications | 
Source | Bending magnet
Energy range | 270-1200 eV
Energy Resolution | Up to 5x10+3
Sample support | TEM grid dual-axis tomography
Li/O2 batteries
Ca Metal batteries
D. S. Tchitchekova, et al. Chem.Mat. 2018 30 (3), 847-856
M.Olivares-Marín, et al.Nano Lett. 2015, 15, 6932−6938

## Slide 30
Steps towards In-situ Microscopy at MISTRAL
Si wafer before dicing
50nm Si3N4 membrane
Mask
Andrea Sorrentino (ALBA)
Dino Tonti (ICMAB)
Francesc Perez-Murano (CNM)
Olga Muntada (CNM)
R. Valcarcel (ALBA)
Victor Fuentes (ICMAB)
Lea Chaptal (ICMAB)
A.Black (ICMAB)
Design of microelectrodes compatible with soft X-ray microscopy operating studies in the MISTRAL beamline (similar to the system already commercially available for transmission electron microscopy).

## Slide 31
Steps towards In-situ Microscopy at MISTRAL
Mn2O4 LiMn2O4 Li2Mn2O4
-Li
+Li
LiMn2O4 Particles
(separation by centrifugation for deposit on electrodes)

## Slide 32
Operando capabilities at Alba Synchrotron

## Slide 33
Battery Laboratory at Alba
PTI+ TRANS-ENER+
Transición Energética Sostenible

## Slide 34
Acknowledgements
PTI+ TRANS-ENER+
Transición Energética Sostenible
MSPD
François Fauth (Alba)
M. Rosa Palacin (ICMAB)
Raphaelle Houdeville (Alba)
Carlos Frontera (ICMAB)
CLAESS
Laura Simonelli (Alba)
Carlo Marini (Alba)
V. Martin-Diaconescu (Alba
Wenhai Wang (ICMAB)
Cheng Liu (ICMAB)
NOTOS
Giovanni Agostini (Alba)
Carlos Escudero (Alba)
Marine Reynaud (CIC)
Marcus Fehse (CIC)
Joseba Orive (CIC)
MIRAS
Ibraheem Yousef (Alba)
Alexandre Ponrouch (ICMAB)
Damien Monti (Alba)
MISTRAL
Andrea Sorrentino (Alba)
Dino Tonti (ICMAB)
Francesc Perez-Murano (CNM)
Olga Muntada (CNM)
Victor Fuentes (ICMAB)
Lea Chaptal (ICMAB)