## Slide 1
X AUSE Conference & V ALBA User’s Meeting 5 – 8 September 2022 ALBA Synchrotron, Barcelona (Spain)
New possibilities of hard X-ray photon-in/photon-out spectroscopies
aESRF – The European Synchrotron;
bInstituto de Nanociencia y Materiales de Aragón (INMA);
cDepartamento de Física de la Materia Condensada, Universidad de Zaragoza
Sara Lafuerzaa,b,c

## Slide 2
Outline
Hard X-ray photon-in/photon-out (PIPO) spectroscopies
  Brief introduction
Range-extended EXAFS
  The edge interference problem
  Examples of applications
A liquid jet setup for RIXS-MCD
  Why applying RIXS-MCD?
  Application to colloidal NPs
Further reading

## Slide 3
Outline
Hard X-ray photon-in/photon-out (PIPO) spectroscopies
  Brief introduction
Range-extended EXAFS
  The edge interference problem
  Examples of applications
A liquid jet setup for RIXS-MCD
  Why applying RIXS-MCD?
  Application to colloidal NPs
Further reading

## Slide 4
1. Hard X-ray PIPO spectroscopies_Brief introduction
PIPO spectroscopies: techniques derived from the combination of XAS-XES
Photon
in
Photon
out
X-ray
Absorption Spectroscopy
X-ray
Emission Spectroscopy
X-ray emission spectrometer
scanning
dispersive
Energy bandwidth ≈ 1 eV

## Slide 5
1. Hard X-ray PIPO spectroscopies_Brief introduction
PIPO spectroscopies: the boom of XES spectrometers
  Hard X-ray spectrometer: ID26, ID20, ROBL (BM20), FAME-UHD (BM16), BM23/ID24, ID09
  Tender X-ray spectrometer: ID26
  Hard X-ray spectrometer: CLAESS
 And many more at other synchrotrons, XFELs and also home laboratories!
Detector
5x analyzer
crystals
Rowland circle
Sample
P. Glatzel et al., J. Synchrotron Rad. 28 362 (2021)
From https://www.cells.es/en/beamlines/bl22-claess

## Slide 6
1. Hard X-ray PIPO spectroscopies_Brief introduction
PIPO spectroscopies with hard X-rays:
  Bulk-sensitivity
  Compatibility with demanding sample environments
EF
3d
L, (3d)
3p
2p
1s
Kα
Kβ
VTC
Kα
Kβ
VTC
NR
NR
R
R
Kα
Kβ
VTC
3p  1s
V  1s
2p  1s
  VTC = valence-to-core
The particular case of K-emission in 3d transition metals:
  - Non-resonant (NR): Ei >> EF
  - Resonant (R): Ei >≈ EF

## Slide 7
1. Hard X-ray PIPO spectroscopies_Brief introduction
X-ray
Absorption Spectroscopy
Ei
If/I0
High Energy Res. Fluo. Detected
Ee @ Kα1 or Kβ1,3
Ee
Kα1
Kα2
If/I0
Ei = 7200 eV
Ee
If/I0
Kβ1,3
Kβ’
Kα
Ge(440)
Kβ
Ge(620)
X-ray
Emission Spectroscopy
I0, Ei
Sample
Si(111) or Si(311)
X-ray emission spectrometer
Incident X-rays
Emitted X-rays
If, Ee
Detector
Analyzer crystals
PIPO spectroscopies with hard X-rays: the umbrella of techniques
e.g. Fe Kα and Kβ XES & Fe K edge HERFD-XAS

## Slide 8
1. Hard X-ray PIPO spectroscopies_Brief introduction
PIPO spectroscopies with hard X-rays: the umbrella of techniques
e.g. Fe 1s2p RIXS @ K pre-edge
Ee
Kα1
Kα2
X-ray
Emission Spectroscopy
Ei
X-ray
Absorption Spectroscopy
If/I0
If/I0
Resonant
Inelastic
X-ray Scattering
1s  3d
1s  4p
High Energy Res. Fluo. Detected
I0, Ei
Sample
Si(111) or Si(311)
X-ray emission spectrometer
Incident X-rays
Emitted X-rays
If, Ee
Detector
Analyzer crystals

## Slide 9
Outline
Hard X-ray photon-in/photon-out (PIPO) spectroscopies
  Brief introduction
Range-extended EXAFS
  The edge interference problem
  Examples of applications
A liquid jet setup for RIXS-MCD
  Why applying RIXS-MCD?
  Application to colloidal NPs
Further reading

## Slide 10
Extended X-ray absorption Fine Structure (EXAFS):
Quantitative information of the local geometrical structure
2. Range-extended EXAFS_The edge interference problem
Coordination number Nj
Interatomic distances Rj
Thermal and static disorder σj2
Photon E  Photo-electron k
EXAFS signal χ(k)
Fe K edge XAS
FeO
XANES
Fe-O
Fe-Fe
k  R
M. Newville, Fundamentals of XAFS, University of Chicago (2004)

## Slide 11
A challenging EXAFS signal extraction:
In multi-element compounds, unfortunate edge interference may occur…
2. Range-extended EXAFS_The edge interference problem
CoFe2O4
M. Bianchini and P. Glatzel, J. Synchrotron. Rad. 19 911 (2012)
Fe K edge
Co K edge
B. Ravel et al., Ferroelectrics 206 407 (1998)
BaTiO3
Positive contribution in TFY & negative contribution in HERFD

HERFD-XAS can help to extend the EXAFS range beyond unwanted edges!

## Slide 12
2. Range-extended EXAFS_Examples of applications
TC≈TMI≈255 K
TN≈TCO≈150 K
H. Kuwahara et al., Science 270 961 (1995)
Experiment at ID26 beamline
Simultaneous TFY- and HERFD-XAS at the Mn Kα1 maximum
Si(311) mono & Ge(333) crystal analyzers  ΔE ≈ 0.4 eV
Continuous He-flow cryostat
Mn local structure in the three magneto-electric phases?
Mn3.5+
Mn4+
Mn3+
Mn K edge EXAFS in mixed-valence Nd0.5Sr0.5MnO3
Half-doped Nd0.5Sr0.5MnO3, a particularly interesting magnetoresistive manganite….

## Slide 13
Mn K edge EXAFS in mixed-valence Nd0.5Sr0.5MnO3
 Interference of Mn K edge (6.5 keV) with Nd L2 edge (6.7 keV)
2. Range-extended EXAFS_Examples of applications
Nd L2 edge
*
      - Linear combination of TFY- and HERFD-XAS data leads to a “range-extended” EXAFS signal
      - The interference with Nd L2 edge would limit the EXAFS range in k-space to only 7 Å-1

## Slide 14
2. Range-extended EXAFS_Examples of applications
Small changes in MnO6 octahedron:
  RMn-O: ↑ until TCO, then stable
  σ2Mn-O: ↓ until TCO, then ↑ with a high value at low T
Mn K edge EXAFS in mixed-valence Nd0.5Sr0.5MnO3
 “Range-extended” EXAFS temperature dependence across the transitions
Mn-O
 dynamic
distortion

↓ distortion
due to long-range FM

↑ distortion
 More information: S. Lafuerza et al., Phys. Rev. B 93 205108 (2016)
PM-I
FM-M
AF-I CO
TC≈TMI
TN≈TCO

## Slide 15
Mn K edge EXAFS in ordered REBaMn2O6 (RE=Nd, Sm)
Polar & magnetic phases ↔ A-site ordered ↔ Controlled synthesis
2. Range-extended EXAFS_Examples of applications
Mn local structure as a function of A-site order, RE-type and temperature?
Experiment at CLAESS beamline
Simultaneous TFY- and HERFD-XAS at the Mn Kβ1,3 maximum
Si(311) mono & Si(333) crystal analyzers  ΔE ≈ 0.5 eV
Liquid-N2 cryostat (80-600 K)
A-site ordered
REBaMn2O3
A-site disordered
RE0.5Ba0.5MnO3
Non-polar
No long-range magnetic order
G. Subías et al., submitted

## Slide 16
2. Range-extended EXAFS_Examples of applications
G. Subías et al., submitted
Mn K edge EXAFS in ordered REBaMn2O6 (RE=Nd, Sm)
 Interference of Mn K edge (6.5 keV) with Nd L2 edge or Sm L3 edge (6.7 keV)
Nd L2 edge
NdBaMn2O3
SmBaMn2O3
Sm L3 edge
*

## Slide 17
2. Range-extended EXAFS_Examples of applications
G. Subías et al., submitted
Mn K edge EXAFS in ordered REBaMn2O6 (RE=Nd, Sm)
 “Range-extended” EXAFS temperature dependence in ordered/disordered samples
A-site ordered
A-site disordered
 More information: Poster by G. Subías “Effects of A-site order on the Mn local structure and polar phases of magnetoelectric REBaMn2O6 (RE: La, Nd, Sm and Y)”

## Slide 18
Outline
Hard X-ray photon-in/photon-out (PIPO) spectroscopies
  Brief introduction
Range-extended EXAFS
  The edge interference problem
  Examples of applications
A liquid jet setup for RIXS-MCD
  Why applying RIXS-MCD?
  Application to colloidal NPs
Further reading

## Slide 19
3. A liquid jet setup for RIXS-MCD_Why applying RIXS-MCD?
1s2p RIXS @ K pre-edge:
1s22p63dn
1s12p63dn+1
1s22p53dn+1
XAS
XES
A site: Td
B site: Oh
Fe3+A[Fe2+,Fe3+]BO2-4
Ee
Ei
Fe3O4
No site-selectivity
Ee
Kα1
Kα2
X-ray
Emission Spectroscopy
Ei
X-ray
Absorption Spectroscopy
If/I0
If/I0
Resonant
Inelastic
X-ray Scattering
1s  3d
1s  4p
High Energy Res. Fluo. Detected

## Slide 20
1s2p RIXS @ K pre-edge
+ X-ray magnetic circular dichroism (RIXS-MCD):
M. Sikora et al., Phys. Rev. Lett. 105 037202 (2010)
Fe3+ Td
Fe2+ Oh
Etransfer = Ei - Ee
Site selectivity!
3. A liquid jet setup for RIXS-MCD_Why applying RIXS-MCD?
A site: Td
B site: Oh
Fe3+A[Fe2+,Fe3+]BO2-4
Fe3O4
N
S
1s22p63dn
1s12p63dn+1
1s22p53dn+1
XAS
XES
Ee
Ei

## Slide 21
  γ-Fe2O3
  (Fe,Mn)3O4
  Mn3O4
1s2p RIXS-MCD: a powerful bulk-sensitive magneto-spectroscopy!
 Fe3O4 buried thin films
M. Sikora et al.,
J. App. Phys. 111 07E301 (2012)
 Core-shell nanoparticles (NPs)
A. Juhin et al.,
Nanoscale 6 11911 (2014)
Soft Core - Hard shell MnFe2O4 @ CoFe2O4 NPs
N. Daffé et al.,
Adv. Mater. Interfaces 4 1700599 (2017)
Ei = 7113.8 eV
Et = 710.8 eV
3. A liquid jet setup for RIXS-MCD_Why applying RIXS-MCD?
Co- and Zn-doped spinel NPs
J. Kuciakowski et al., Nanoscale 12 16420 (2020)

## Slide 22
Colloidal magnetic nanoparticles (NPs):
  Sufficiently small NPs  superparamagnetic at room temperature (ferromagnetic at cryogenic temperatures)
  Very promising for biomedical applications, especially in cancer therapies (e.g. hyperthermia, photothermia, …)
  Iron oxide-based NPs are the preferred materials due to its biocompatibility
Characterization of colloidal NPs useful only under in situ conditions,
i.e. directly in the carrier liquid at room temperature

Liquid jet setup for in situ RIXS-MCD
S. Shen et al., Nanoscale 5 8056 (2013)
3. A liquid jet setup for RIXS-MCD_Application to colloidal NPs
M. Mehrmohammadi et al., Nanotechnology 22 045501 (2011)

## Slide 23
Main components and requirements for RIXS-MCD liquid jet:
Pump
Magnet
 Small split coil electromagnet
@ ESRF Sample Environment Support Service
Ø 120 mm
6 mm gap
Water cooling
Beam access Ø 2 mm
±0.5 Tesla peak (±5.5 A)
Peltier stage for temperature control
 Rotatory gear pump
Brushed DC electric motor
Outlet
Inlet
mzr-11508X1 model, HNP Mikrosysteme GmbH
Generally resistant to solvents (pH > 4)
Flow rate: 0.2 – 1000 ml/min
3. A liquid jet setup for RIXS-MCD_Application to colloidal NPs
Suitable for magnetic fluids ( Magnetic drive gear pump)
Continuous flow ( Peristaltic pump)
Compact and suited for X-ray fluorescence geometry
Field sweep and reversal ( Permanent magnet)

## Slide 24
Emitted X-rays
H
Electro-magnet
Stirrer
Reservoir
Free jet
The liquid jet setup for RIXS-MCD at ID26 beamline (ESRF)
Incident x-rays
Rotatory gear pump
Si(311) mono.
Circular polarization (diamond phase plate)
I0, Ei
If, Ee
Sample volume:
≈ 30 ml
3. A liquid jet setup for RIXS-MCD_Application to colloidal NPs
X-ray emission spectrometer

## Slide 25
First RIXS-MCD experiment in the liquid jet setup
Samples: commercial nominally Fe3O4 NPs
20 nm
5 nm
TEM images courtesy of A. G. Roca
3. A liquid jet setup for RIXS-MCD_Application to colloidal NPs
      - Spherical NPs of 20, 10 and 5 nm diameter synthesized by thermal decomposition and dispersed in toluene (Sigma-Aldrich)
 Kα1-detected Fe K edge HERFD-XANES
      - Main edge: ↓ size  ↑ oxidation
      - Pre-edge: ↓ size  ↓ Fe2+, ↑ Fe3+
Fe3O4
(Fe3+Td[Fe2+,Fe3+]OhO2-4)
 γ-Fe2O3
(Fe3+Td[Fe3+ 5/31/3]OhO2-4)
Fe2+
Fe3+
F. M. F. de Groot et al.,
J. Phys. Chem. B 109 20751 (2005)
Oh
Td
Td
Oh
Fe2+
Fe3+

## Slide 26
First RIXS-MCD experiment in the liquid jet setup
Fe3O4
γ-Fe2O3
3. A liquid jet setup for RIXS-MCD_Application to colloidal NPs
 RIXS-MCD maps & diagonal cuts
Fe2+ Oh
Fe3+ Td
      - Line-shape: 20 nm≈Fe3O4, 5 nm≈γ-Fe2O3
      - Amplitude: NPs < bulk & 20 nm < 5nm, poorer crystallinity of 20 nm sample?
Fe3O4
γ-Fe2O3

## Slide 27
Outline
Hard X-ray photon-in/photon-out (PIPO) spectroscopies
  Brief introduction
Range-extended EXAFS
  The edge interference problem
  Examples of applications
A liquid jet setup for RIXS-MCD
  Why applying RIXS-MCD?
  Application to colloidal NPs
Further reading

## Slide 28
4. Further reading
S. P. Cramer, 2020 Photon-in Photon-out Spectroscopy, X-Ray Spectroscopy with Synchrotron Radiation Fundamentals and Applications (Springer) Chapter 8
P. Glatzel et al., 2016 Hard X-Ray Photon-in/Photon-out Spectroscopy: Instrumentation, Theory and Applications, X-ray Absorption and X-Ray Emission Spectroscopy: Theory and Applications (Wiley) Chapter 6
P. Glatzel et al., 2014 X-ray Absorption and Emission Spectroscopy, Local Structural Characterization Inorganic Materials Series (Wiley) Chapter 2
Reviews:
S. Lafuerza et al. New reflections on hard X-ray photon-in/photon-out spectroscopy. Nanoscale 12 16270 (2020)
M. Rovezzi et al. Hard x-ray emission spectroscopy: a powerful tool for the characterization of magnetic semiconductors. Semicond. Sci. Technol. 29 023002 (2014)
P. Glatzel et al. High resolution 1s core hole X-ray spectroscopy in 3d transition metal complexes—electronic and structural information. Coord. Chem. Rev. 249 65 (2005)
Book chapters:

## Slide 29
Acknowledgements
G. Subías, J. García, J. Blasco & V. Cuartero
P. Glatzel
B. Detlefs
T. Bohdan
Liquid jet setup for RIXS-MCD
Range-extended EXAFS
Thank you
for your attention!
P. Van der Linden (ESRF)
Y. Watier (ESRF)
J. Nogués
A. G. Roca
J. Muro-Cruces
G. Gorni & L. Simonelli
V. Puntes
M. Busquets-Fité
J. Piella
M. Rovezzi (CNRS)
H. Elnaggar (Sorbonne Université)

## Slide 30
X AUSE Conference & V ALBA User’s Meeting 5 – 8 September 2022 ALBA Synchrotron, Barcelona (Spain)
New possibilities of hard X-ray photon-in/photon-out spectroscopies
aESRF – The European Synchrotron;
bInstituto de Nanociencia y Materiales de Aragón (INMA);
cDepartamento de Física de la Materia Condensada, Universidad de Zaragoza
Sara Lafuerzaa,b,c

## Slide 31
1. Hard X-ray PIPO spectroscopies_Brief introduction
The hard X-ray emission spectrometer at ID26
X-rays
Detector
5x analyzer
crystals
Rowland circle
Sample
Point-to-point scanning Johann vertical spectrometer
Rowland circle geometry (1 or 0.5 m)
Bragg angle (θ): 65° - 85°
Energy range: 4.5 – 17 keV
Energy resolution: ~ 1 eV
5x spherical crystals
Si <400>
Si <220>
Si <111>
Si <531>
Si <551>
Si <951>
Si <620>
Si <311>
Si <422>
Ge <400>
Ge <220>
Ge <111>
Ge <620>
Ge <311>
Ge <422>
P. Glatzel et al.,
J. Synchrotron Rad. 28 362 (2021)

## Slide 32
2. Range-extended EXAFS_Examples of applications
G. Subías et al., submitted
Mn K edge EXAFS in ordered REBaMn2O6 (RE=Nd, Sm)
 “Range-extended” EXAFS temperature dependence in ordered/disordered samples
A-site ordered
A-site disordered

## Slide 33
First RIXS-MCD experiment in the liquid jet setup
3. A liquid jet setup for RIXS-MCD_Application to colloidal NPs
 Site-selective hysteresis loops at selected MCD features
Fe3+ Td
Fe2+ Oh