## Slide 1: Magnetic and electronic properties of 2D metal-organic networks
Sofia de Oliveira Parreiras
sofia.oliveira@imdea.org

## Slide 2: Molecular magnetism
High potential for technological applications
  High density information storage
  Molecular spin qubits
  Spintronics devices
Low dimensional materials
  Novel quantum properties
2D metal-organic networks
  Long range ordering
π-conjugated metal-organic networks
Lanthanide metal-organic networks
Molecules
Metal
Surface
On-surface synthesis

## Slide 3: Magnetism of metal-organic networks
Phys. Rev. Lett. 2012, 109, 267207
Fe-T4PT/Au(111)
Ferromagnetic coupling
Ni-TCQN/Au(111)
Mn-TCQN/Au(111)
Phys. Rev. Lett. 2013, 110, 027202
J Phys. Chem. C 2015, 119, 547-555
Ferromagnetic coupling
Weak antiferromagnetism

## Slide 4: Experimental setups
XAS, XLD, XMCD, STM
ALBA synchrotron
STM, STS, nc-AFM
IMDEA Nanoscience

## Slide 5: π-conjugated metal-organic networks

## Slide 6
Exotic quantum phases of matter
  Superconductivity
  Quantum anomalous Hall effect
  Flat-band
Antiferromagnetic ground-states
  Absence of stray fields
  Magnetic robustness
  Ultrafast dynamics
Truly 2D systems
  Networks prepared by on-surface synthesis
  Reduction of the coordination of number
  Route to unquenched orbital moment
π-conjugated metal-organic networks
3d metal:
Co
Light blue: carbon; Gray: hydrogen; Red: oxygen
HOTP
2,3,6,7,10,11-Hexahydroxytriphenylene
HOB
1,2,3,4,5,6-hexahydroxybenzene
Molecular linkers:
M. Ko et al., Chem.Commun., 2018, 54, 7873
2D layered networks

## Slide 7
STM image
STM image + model
nc-AFM image
Co-HOB metal-organic network
Vb = -500 mV, I = 800 pA,
T = 4 K, 5 nm x 5 nm
Vb = -500 mV, I = 800 pA,
T = 4 K, 5 nm x 5 nm
Constant height,
Vb = 5mV, T = 4 K, 2 nm x 2 nm
HOB
Co
+
Au(111)

## Slide 8
Electronic properties: Co-HOB
0.14 V
Semiconductor with very low bangap

## Slide 9: Magnetic properties: Co-HOB
0°
70°
L3
L2
6 T
Energy (eV)
Total Electron Yield (norm. unit)
XMCD (norm. unit)
Magnetic moments (nH=3)
Strong in-plane magnetic anisotropy
  Unquenched orbital moment
  Large orbital to effective spin moment
Magnetization curves compatible with paramagnetism or antiferromagnetism
Incidence angle (º) | (ℏ) | (ℏ) | (μB) | (μB) | 
70 | 0.22 (2) | 0.29 (3) | 0.43 (4) | 0.29 (3) | 0.67(7)
0 | 0.06 (1) | 0.07 (1) | 0.12 (2) | 0.07 (1) | 0.58(8)
Incidence angle (º) |  |  |  |  | 
70 | 0.22 (2) | 0.29 (3) | 0.43 (4) | 0.29 (3) | 0.67(7)
0 | 0.06 (1) | 0.07 (1) | 0.12 (2) | 0.07 (1) | 0.58(8)
Field (T)
Intensity (norm. unit)

## Slide 10
-0.5
1.2
df (Hz)
STM image
STM image + model
nc-AFM image
nc-AFM simulation
Co-O coordination: 3-fold
Two molecular species: 4-fold and 6-fold
Co-HOTP metal-organic network
Vb = 20 mV, I = 100 pA,
T = 4 K, 4 nm x 4 nm
Vb = 20 mV, I = 120 pA,
T = 4 K, 11.7 nm x 11.7 nm
Open feedback: Vb = 5mV, It = 150 pA, Zoffset = 150 pm,T = 4 K, 3.2 nm x 3.2 nm
HOTP
Co
+
Au(111)

## Slide 11
Electronic properties: Co-HOTP
STS
DFT+U
0.25 V
30 mV
0.28 V
0.29 V
6-fold molecule
-0.9 V
4-fold molecule
-0.7 V
Semiconductor with very low bangap

## Slide 12: Magnetic properties: Co-HOTP
Field (T)
Intensity (norm. unit)
Incidence angle (º) | (ℏ) | (ℏ) | (μB) | (μB) | 
70 | 0.61 (6) | 0.98 (10) | 1.22 (12) | 0.98 (10) | 0.80(11)
0 | 0.14 (1) | 0.19 (2) | 0.28 (3) | 0.19 (2) | 0.68(10)
Incidence angle (º) |  |  |  |  | 
70 | 0.61 (6) | 0.98 (10) | 1.22 (12) | 0.98 (10) | 0.80(11)
0 | 0.14 (1) | 0.19 (2) | 0.28 (3) | 0.19 (2) | 0.68(10)
0°
70°
L3
L2
6 T
Energy (eV)
Total Electron Yield (norm. unit)
XMCD (norm. unit)
Magnetic moments (nH=2.74, DFT)
Strong in-plane magnetic anisotropy
  Large unquenched orbital moment
  Large orbital to effective spin moment
Magnetization curves compatible with paramagnetism or antiferromagnetism

## Slide 13: Magnetic properties: Co-HOTP
In-plane antiferromagnetic

## Slide 14: Magnetic properties: Co-HOTP
In-plane antiferromagnetic
Field (T)
Intensity (norm. unit)
0°
70°
L3
L2
6 T
Energy (eV)
Total Electron Yield (norm. unit)
XMCD (norm. unit)
In-plane anisotropy
Compatible with antiferromagnetism

## Slide 15: Summary: π-conjugated metal-organic networks
On-surface synthesis of a Co-coordinated metal-organic networks on Au(111)
Semiconductors with very low bandgaps
Antiferromagnetic ground state
Large unquenched orbital magnetic moment and large orbital to effective spin moment ratio
  Unprecedented in 2D transition metal-organic architectures

## Slide 17: Lanthanides metal-organic networks

## Slide 18: Magnetism of lanthanides
Magnetic remanence in single atoms
F. Donati et al., Science 2016, 352, 318-321
Writing and reading single atoms
F. Natterer et al., Nature 2017, 543, 226-228
Strong spin-orbit coupling
Strong localization of 4f states
High magnetic moments and magnetic anisotropy
Large spin lifetimes

## Slide 19: Lanthanide metal-organic networks
4f metals:
Dy
Er
Dy+3
oblate charge density
Er+3
prolate charge density
Light blue: carbon; Gray: hydrogen; Red: oxygen; Dark blue: Nitrogen
TDA
p-terphenyl-4,4-dicarboxylic acid
DPBP
4,4'-di(pyridin-4-yl)-1,1'-biphenyl
Molecular linkers:

## Slide 20: Dinuclear networks: Dy-DPBP and Er-DPBP
Vb = -300 mV, I = 1.5 nA, CO tip
T = 4 K, Scale bar: 2.0 nm
Vb = -1.00 V, Zoffset = -94 pm, CO tip
T = 4 K, Scale bar: 1.0 nm
Vb = 100 mV, I = 3.0 nA,
T = 4 K, Scale bar: 2.0 nm
Vb = 500 mV, I = 200 pA,
T = 4 K, Scale bar: 3.0 nm
Vb = 5 mV, I = 50 pA, CO tip
T = 4 K, Scale bar: 1.0 nm
DPBP
Er
+
Au(111)
DPBP
Dy
+
Au(111)

## Slide 21: Electronic properties: Dy-DPBP and Er-DPBP

## Slide 22: Magnetic properties: Rhombic networks
DPBP
Er
+
Au(111)
DPBP
Dy
+
Au(111)
0°
70°
0°
70°
0°
70°
0°
70°
Multiplet calculations:
MultiX
A. Uldry et al., Phys. Rev. B 2012, 85, 125133
Dy+3
Er+3

## Slide 23: Magnetic properties: Rhombic networks
DPBP
Dy
+
Au(111)
DPBP
Er
+
Au(111)
50°
80°
Multiplet calculations:
MultiX
A. Uldry et al., Phys. Rev. B 2012, 85, 125133
Incidence angle | Er centers on DPBP networks |  | Dy centers on DPBP networks | 
 | 0º () | 70º | 0º () | 70º
(ħ) | 4.69(47) | 3.89(39) | 1.91(19) | 4.46(45)
(ħ) | 1.00(10) | 0.95(10) | 0.99(10) | 1.99(20)
 | 5.69(57) | 4.84(48) | 2.90(29) | 6.45(64)
(B/atom) | 6.70(67) | 5.79(58) | 3.88(39) | 8.44(84)
(B/atom) | -0.9(1.3) |  | 4.6(1.2) | 
Incidence angle | Er centers on DPBP networks |  | Dy centers on DPBP networks | 
 |  | 70º |  | 70º
 | 4.69(47) | 3.89(39) | 1.91(19) | 4.46(45)
 | 1.00(10) | 0.95(10) | 0.99(10) | 1.99(20)
 | 5.69(57) | 4.84(48) | 2.90(29) | 6.45(64)
 | 6.70(67) | 5.79(58) | 3.88(39) | 8.44(84)
 | -0.9(1.3) |  | 4.6(1.2) | 

## Slide 24: Mononuclear networks: Dy-TDA and Er-TDA
TDA
Er
+
Cu(111)
Vb = -0.80 V, I = 150 pA,
T = 4 K, Scale bar: 1.0 nm
Vb = 500 mV, I = 500 pA,
T = 4 K, Scale bar: 2.0 nm
TDA
Dy
+
Cu(111)

## Slide 25
0°
70°
M5
6 T
M4
Energy (eV)
Total Electron
Yield (norm. u.)
XMCD (norm. u.)
TDA
Er
+
Cu(111)
A. Singha et al., Phys. Rev. B 2017, 96, 224418
Magnetic properties: Dy-TDA and Er-TPA
Dy+2
Er+3
In-plane
TDA
Dy
+
Cu(111)
Dy+3
Nearly in-plane
M5
M4
6 T
0°
70°
Energy (eV)
Total Electron
Yield (norm. u.)
XMCD (norm. u.)
Er+3
Out-of-plane
Magnetic Field (T)
Intensity
Single atoms
Magnetic Field (T)
Intensity (norm. unit)
Almost Isotropic
 = 71.2°

## Slide 26: Expectation values of magnetic moments
Incidence angle | Dy centers on TDA networks |  | Dy single atoms on Cu(111)* |  | Er centers on TDA networks |  | Er single atoms on Cu(111)* | 
 | 0º () | 70º | 0º () | 60º | 0º () | 70º | 0º () | 60º
(ħ) | 1.36 (14) | 2.35 (24) | 4.7 (2) | 4.4 (2) | 6.08(61) | 3.05(31) | 0.7(1) | 4.0(2)
(ħ) | 0.44 (4) | 1.14 (11) | 1.6 (1) | 1.5 (0) | 1.79(18) | 0.91(9) | 0.3(0) | 1.0(1)
 | 1.80 (18) | 3.49 (35) | 6.3 (2) | 5.9 (2) | 7.87(79) | 3.96(40) | 1.0(1) | 5.0(2)
(B/atom) | 2.24 (22) | 4.63 (46) | 7.9 (3) | 7.4 (2) | 9.66(97) | 4.87(49) | 1.3(1) | 6.0(3)
(B/atom) | 2.4 (7) |  | -0.5 (5) |  | -4.8(1.5) |  | 4.7(4) | 
Incidence angle | Dy centers on TDA networks |  | Dy single atoms on Cu(111)* |  | Er centers on TDA networks |  | Er single atoms on Cu(111)* | 
 |  | 70º |  | 60º |  | 70º |  | 60º
 | 1.36 (14) | 2.35 (24) | 4.7 (2) | 4.4 (2) | 6.08(61) | 3.05(31) | 0.7(1) | 4.0(2)
 | 0.44 (4) | 1.14 (11) | 1.6 (1) | 1.5 (0) | 1.79(18) | 0.91(9) | 0.3(0) | 1.0(1)
 | 1.80 (18) | 3.49 (35) | 6.3 (2) | 5.9 (2) | 7.87(79) | 3.96(40) | 1.0(1) | 5.0(2)
 | 2.24 (22) | 4.63 (46) | 7.9 (3) | 7.4 (2) | 9.66(97) | 4.87(49) | 1.3(1) | 6.0(3)
 | 2.4 (7) |  | -0.5 (5) |  | -4.8(1.5) |  | 4.7(4) | 
Strong moment anisotropy
*A. Singha et al., Phys. Rev. B 2017, 96, 224418

## Slide 27: Summary: Lanthanides metal-organic networks
Unprecedented mononuclear and dinuclear lanthanide-directed metal-organic networks designed by on-surface chemistry
By metal-exchange:
  Network integrity
  Tailoring of energy level alignment
  Drastic modification of magnetic properties
It is possible to tailor the magnetic anisotropy of lanthanide elements on surfaces by coordinative metal-organic protocols

## Slide 29: Thanks for your attention!
IMDEA Nanoscience
Prof. David Écija
Prof. Rodolfo Miranda
Dr. Paolo Perna
Prof. Julio Camarero
Dr. Daniel Moreno
Dr. Borja Cirera
Dr. Miguel A. Valbuena
Dr. José I. Urgel
Dr. Koen Lauwaet
Beatriz Muñiz-Cano
Dr. José M. Gallego
Dr. Miguel A. Niño
Cristina Martín-Fuentes
Dr. Fernando Ajejas
ALBA synchroton
Dr. Pierluigi Gargiani
Dr. Manuel Valvidares
ICMol Universitat de València
Prof. Carlos Martí-Gastaldo
Dr. Victor Rubio-Giménez
ICN2
Prof. Aitor Mugarza
Dr. Markos Paradinas
Dr. Mirco Panighel
ICMM-CISC
Dr. José I. Martínez
Freie Universität
Prof. Wolfgang Kuch
sofia.oliveira@imdea.org
Nanoarchtectonics on Surfaces Group

## Slide 30
Electronic properties: Co-HOTP
6-fold molecule
-0.9 V
4-fold molecule
-0.7 V
STS
dI/dV maps

## Slide 31: Oxidation state
L3
L2
6 T
Energy (eV)
Total Electron Yield (norm. unit)
Intensity (arb. unit)
Intensity (arb. unit)
Intensity (arb. unit)
Energy (eV)
Energy (eV)
Energy (eV)
Energy (eV)
a)
b)
c)
d)
e)
Intensity (arb. unit)
This work
Co+3
Co+2

## Slide 32: Electronic properties: Dy-TDA and Er-TDA
TDA
Er
+
Cu(111)
TDA
Dy
+
Cu(111)
dI/dV (arb. u.)
Bias (V)
Vb = -0.70 V, I = 80 pA,
T = 4 K, Scale bar: 3.0 nm
Topography
dI/dV map
Vb = -0.20 V, I = 80 pA,
T = 4 K Scale bar: 1.0 nm
1.6 V
dI/dV (arb. u.)
Bias (V)
Topography
dI/dV map
Vb = 1.73 V, I = 200 pA,
T = 4 K Scale bar: 2.0 nm
Topography
dI/dV map
Vb = 2.67 V, I = 200 pA,
T = 4 K Scale bar: 2.0 nm
1.7 V
2.7 V
Vb = 500 mV, I = 500 pA,
T = 4 K, Scale bar: 3.0 nm

## Slide 33: Dy-TDA: Background subtraction
Energy (eV)
Total Electron Yield (arb. u.)
XMCD (arb. u.)
Total Electron Yield (norm. u.)
XMCD (norm. u.)
Energy (eV)
M5
M4
M5
M4

## Slide 34: Mononuclear networks: Dy-TDA and Dy-TPA
TPA
Dy
+
Cu(111)
TDA
Dy
+
Cu(111)
Vb = -0.80 V, I = 150 pA,
T = 4 K, Scale bar: 1.0 nm
Vb = -1.10 V, I = -170 pA,
T = 300 K, Scale bar: 1.0 nm

## Slide 35
DPBP
Er
+
Au(111)
DPBP
Dy
+
Au(111)
TDA
Dy
+
Cu(111)
TDA
Er
+
Cu(111)
TPA
Dy
+
Cu(111)
Energy (eV)
M5
0.01 T
XAS
(norm. u.)
XNLD
(norm. u.)
XAS
(norm. u.)
XNLD
(norm. u.)
Energy (eV)
M5
0.01 T
Energy (eV)
XAS
(norm. u.)
XNLD
(norm. u.)
M5
0.01 T
M5
0.05 T
Energy (eV)
XAS
(norm. u.)
XNLD
(norm. u.)
M5
0.05 T
Energy (eV)
XAS
(norm. u.)
XNLD
(norm. u.)
70°
70°
70°
70°
70°

## Slide 36: Magnetic properties: Dy-TDA and Dy-TPA
TPA
Dy
+
Cu(111)
TDA
Dy
+
Cu(111)
Nearly in-plane
anisotropy
0°
70°
M5
6 T
M4
Energy (eV)
XAS (norm. u.)
XMCD
(norm. u.)
Magnetic Field (T)
Intensity
Magnetic Field (T)
Intensity
XAS (norm. u.)
XMCD
(norm. u.)
Energy (eV)
0°
70°
M5
6 T
M4
 = 72.9°
 = 71.2°

## Slide 37: Expectation values of magnetic moments
Incidence angle | Dy centers on TDA networks |  | Dy centers on TPA networks |  | Dy single atoms on Cu(111)* |  | Er centers on TDA networks |  | Er single atoms on Cu(111)* | 
 | 0º () | 70º | 0º () | 70º | 0º () | 60º | 0º () | 70º | 0º () | 60º
(ħ) | 1.36 (14) | 2.35 (24) | 1.00 (10) | 2.77 (28) | 4.7 (2) | 4.4 (2) | 6.08(61) | 3.05(31) | 0.7(1) | 4.0(2)
(ħ) | 0.44 (4) | 1.14 (11) | 0.60 (6) | 1.18 (11) | 1.6 (1) | 1.5 (0) | 1.79(18) | 0.91(9) | 0.3(0) | 1.0(1)
 | 1.80 (18) | 3.49 (35) | 1.60 (16) | 3.95 (40) | 6.3 (2) | 5.9 (2) | 7.87(79) | 3.96(40) | 1.0(1) | 5.0(2)
(B/atom) | 2.24 (22) | 4.63 (46) | 2.20 (22) | 5.13 (51) | 7.9 (3) | 7.4 (2) | 9.66(97) | 4.87(49) | 1.3(1) | 6.0(3)
(B/atom) | 2.4 (7) |  | 2.9 (7) |  | -0.5 (5) |  | -4.8(1.5) |  | 4.7(4) | 
Incidence angle | Dy centers on TDA networks |  | Dy centers on TPA networks |  | Dy single atoms on Cu(111)* |  | Er centers on TDA networks |  | Er single atoms on Cu(111)* | 
 |  | 70º |  | 70º |  | 60º |  | 70º |  | 60º
 | 1.36 (14) | 2.35 (24) | 1.00 (10) | 2.77 (28) | 4.7 (2) | 4.4 (2) | 6.08(61) | 3.05(31) | 0.7(1) | 4.0(2)
 | 0.44 (4) | 1.14 (11) | 0.60 (6) | 1.18 (11) | 1.6 (1) | 1.5 (0) | 1.79(18) | 0.91(9) | 0.3(0) | 1.0(1)
 | 1.80 (18) | 3.49 (35) | 1.60 (16) | 3.95 (40) | 6.3 (2) | 5.9 (2) | 7.87(79) | 3.96(40) | 1.0(1) | 5.0(2)
 | 2.24 (22) | 4.63 (46) | 2.20 (22) | 5.13 (51) | 7.9 (3) | 7.4 (2) | 9.66(97) | 4.87(49) | 1.3(1) | 6.0(3)
 | 2.4 (7) |  | 2.9 (7) |  | -0.5 (5) |  | -4.8(1.5) |  | 4.7(4) | 
Strong moment anisotropy
*A. Singha et al., Phys. Rev. B 2017, 96, 224418

## Slide 38: Theoretical fitting of magnetization curves
Parameter | Dy clusters in Cu(111) | Dy centers in TDA networks | Dy centers in TPA networks
T (K) | 6.8 | 6.0 | 6.3
 (°) | 65.0 | 71.2 | 72.9
D (meV) | -9.98 | -10 (-) | -10 (-)
a | 0.58 | 0.57 | 0.56
Parameter | Dy clusters in Cu(111) | Dy centers in TDA networks | Dy centers in TPA networks
T (K) | 6.8 | 6.0 | 6.3
 (°) | 65.0 | 71.2 | 72.9
D (meV) | -9.98 |  | 
a | 0.58 | 0.57 | 0.56
Dy-TDA
Magnetic Field (T)
 = 71.2°
Dy-TPA
Magnetic Field (T)
 = 72.9°
Dy clusters
Magnetic Field (T)
Intensity
 = 65.0°