## Slide 1
Simon Wall
ICFO – The Institute for Photonic Science
Barcelona
Spain
Paris 2017
Understanding quantum materials by their non-equilibrium dynamics
Notes: Insulator-metal phase transitions have a huge promise for future technologies because very large changes in material properties, such as the conductivity, or optical can occur. Some materials can also effect this change very rapidly. However, the mechanisms behind many of these transitions are still poorly understood. They key interactions are between the electrons and the phonons which control how the energy imparted by light is redistributed in the material. Today I am going to talk about how we can watch dynamics of the insulator-metal phase transitions in order to try and understand how and why these phase transitions occur in two contrasting systems.

## Slide 2: Quantum Materials
Wahl, Nat. Phys. (2012)
CDW
Millis Nature (1998)
Cuprates
Manganites
Initial phases are anti-ferromagnetic insulators
Suggests Mott-Hubbard physics and strong electronic correlation
Charge density wave states emerge with doping
Suggests Peierls-like physics and strong electron-phonon coupling
Do electron-electron or electron-phonon interactions dominate the physics of quantum materials?

## Slide 3: How can ultrafast help?
Requirement: Source to transfer energy to electrons (and thermalize) before energy is transferred to the lattice – femtosecond timescale
n
E
n
E
n
E

## Slide 4: Probing material dynamics
F = 1 kHz, T = 1/F = 1 ms
Measuring reversible dynamics using Pump-Probe technique
Pump
Probe
X = 2c Δt
Δt
Δt
Stroboscopic technique.
Laser fires a pulse at a constant repetition rate
Measure one delay many times
sample
t
Notes: How we probe what happened in the femtosecond timescales

## Slide 5: Probing femtosecond dynamics
Pump
Probe
X = 2c Δt
Δt
Δt
t
Measure one delay many times
Move delay and repeat
Measuring reversible dynamics using Pump-Probe technique
F = 1 kHz, T = 1/F = 1 ms
sample
Probe can be:
Optical pulse
X-rays
Electrons…
Notes: How we probe what happened in the femtosecond timescales

## Slide 6: Ge2Sb2Te5
Non – quantum material with light-induced insulator-metal transition

## Slide 7: Crystalline-Amorphous Phase Transformation
Crystalline
Amorphous
Transformation can occur with a single 35 fs laser pulse
Transformation quasi-reversible
L. Waldecker et al. Nature Materials. 14, 991 (2015)

## Slide 8: Reversible Femtosecond dynamics
Crystalline
Amorphous
0.05 mJ/cm2
6 mJ/cm2
Delay / ps
Delay / ps
Delay / ps
Delay / ps
Picosecond recovery dynamics + long lived component
Acoustic phonon (breathing of the film)
(Special) Coherent optical phonons

## Slide 9: Ultrafast processes in a semiconductor
VB
CB
Photo-excitation creates a charge distribution in the conduction band

## Slide 10: Ultrafast processes in a semiconductor
VB
CB
(A semiconductor perspective)
Photo-excitation creates a charge distribution in the conduction band
Electrons thermalize
Electrons cool to the minimum of the conduction band emitting phonons and heating the lattice
Is the band structure rigid?

## Slide 11: Ultrafast processes in a semiconductor
VB
CB
Bonding
Anti-bonding
Change in charge distribution can apply a force on lattice – Strongly Coupled Optical Phonons
Phonon
Force/electrons
Time
Amplitude/population
e
SCOP
lattice

## Slide 12: Ultrafast processes in a semiconductor
VB
CB
Bonding
Anti-bonding
Change in charge distribution can apply a force on lattice – Strongly Coupled Optical Phonons
Short Pulse excitation can generate coherent phonons
Time
Amplitude/population
Phonon
Force/electrons
e
SCOP
lattice

## Slide 13: Measuring the Structure
Electron Lens
Sample on
TEM grid
80 kV
30 fs VIS laser pulse
Pump Laser
L. Waldecker et al. J Appl. Phys. 117, 044903 (2015)
L. Waldecker et al. Nature Materials. 14, 991 (2015)

## Slide 14: Measuring the Structure
Electron Lens
Sample on
TEM grid
80 kV
30 fs VIS laser pulse
Pump Laser
L. Waldecker et al. Nature Materials. 14, 991 (2015)

## Slide 15: Measuring the Structure
Electron Lens
Sample on
TEM grid
80 kV
30 fs VIS laser pulse
Pump Laser
L. Waldecker et al. Nature Materials. 14, 991 (2015)

## Slide 16: Above Threshold Dynamics
L. Waldecker et al. Nature Materials. 14, 991 (2015)
Lattice response remains thermal
Melting occurs in ~ 5ps
Resulting phase is a liquid
Amorphization occurs during rapid cooling

## Slide 17: VO2
Metallic Rutile R-phase
Insulating Monoclinic M1-phase
V ions “pair and twist”

## Slide 18: Controversial Topic
V 3d
V 3d//
Ef
M1
R
V 3d
V 3d//
Ef
Monoclinic metal
R
Mott insulator

## Slide 19: The Photoinduced Phase Transition in VO2
Light can drive the insulator-metal transition
Below threshold – Material remains monoclinic
Threshold – Start of metallization
Saturation – Complete transformation
Thermal diffusion restores monoclinic insulating phase in ~1 ns
Pump: 800 nm
Probe: 5 µm
Delay: 1 ps
Sample: Thin film
1
2
3

## Slide 20: Timescale for the Phase Transition
Optical:
75 fs = ½ period of one Ag Raman active phonon
Diffraction:
470 160 fs Cavalleri et al. PRL. 87 (2001)
307 fs Baum et al. Science 318 (2007)
310 160 fs Morrison et al. Science 346 (2015)
Photoemission:
Instantaneous gap collapse

## Slide 21: Identifying a Phase
Average atomic positions –Bragg peaks
Morrison et al. Science (2015)
Jones et al. Nano letters (2010)
Phonon modes – Raman Spectrum

## Slide 22: M1 Phase Response to Photoexcitation
800 nm
525 nm
S. Wall et al. Nature communications 3 721 (2012)
Experimental Details
Pump: 800 nm
Probe: White light
Pump fluence: < FTH
Sample: Thin film
T = Room Temperature

## Slide 23: M1 Phase Response to Photoexcitation
5.6 THz
6.7 THz
800 nm
525 nm
S. Wall et al. Nature communications 3 721 (2012)

## Slide 24: R Phase Response to Photoexcitation
No oscillations – as expected
Experimental Details
Pump: 800 nm
Probe: White light
Pump fluence: < FTH
Sample: Thin film
T = 400 K
S. Wall et al. PRB 87 115126 (2013)

## Slide 25: Phase change dynamics
S. Wall et al. Nature communications 3 721 (2012)
F< FTH
F> FTH
800 nm
525 nm
ΔR/R

## Slide 26: Phase Change Dynamics
S. Wall et al. Nature communications 3 721 (2012)
?

## Slide 27: Measuring Phonons With X-rays
+
+ …
Bragg peaks
Thermal diffuse scattering
Response dominated by low frequency modes
Budai et al. Nature 515, 535 (2014)
Vibrations of uncorrelated Vanadium ions

## Slide 28: Time-Resolved TDS
D. Zhu et al. Phys Rev B. 92, 054303 (2015)

## Slide 29: Time-Resolved TDS F>FTH
High Temperature
Transient change
Low Temperature

## Slide 30: Time Resolved TDS F>FTH
0 fs
4 ps
8 ps

## Slide 31: Fluence Dependence
0 fs
Diffuse Scattering
Bragg “Peak”
Diffuse scattering associated with random vanadium dimer oscillations only appears at the phase transition
A
B

## Slide 32: Time Dependence
A
B
A
B
Rutile like vibrations emerge after ~50 fs
Lattice thermalization time may be as fast as electron thermalization!

## Slide 33: Spin dynamics in manganites
LaMnO3 – Parent compound for magnaites
Static Jahn-Teller distortion in ab-plane below TJT = 780 K
A-type anti-ferromagnetism TN = 140 K
J>0
a
b
S Wall et al PRL 103 09742 (2009)
Notes: Start with the parent compound. Does not exhibit dynamic phase transition, but is a cleaner compound in the sense that we know a lot about it.
Explain structure + Magnetic state.
AF = Pauli
F = Hund

## Slide 34: Coherent Phonons in LaMnO3
Jahn-Teller
Stretching
14.9 THz
61.5 meV
497 cm-1
Out-of-phase bending
8.8 THz
36.3 meV
293 cm-1
S Wall et al PRL 103 09742 (2009)

## Slide 35: Phonon-Magnon Coupling
Anharmonic decay of to acoustic phonons:
Anharmonic decay of to magnons:
Energy transfer between phonons and spins in ~250 fs
Are electrons or phonons more effective at driving demagnetization?
Bend
JT
Bend
JT
S Wall et al PRL 103 09742 (2009)
Notes: As a result we expect to see some coupling between lattice and the structure and this is seen in the dynamics.

## Slide 36: Phonon-Magnon Coupling
Energy transfer between phonons and spins in ~250 fs
Are electrons or phonons more effective at driving demagnetization?
e
SCOP
lattice
spin
Notes: As a result we expect to see some coupling between lattice and the structure and this is seen in the dynamics.

## Slide 37: Measuring Antiferromagnetic Dynamics
Ferromagnetism breaks time-reversal symmetry
Left/right circularly polarized light absorbed differently
Magnetic dynamics can be monitored by tracking the L/R absorption
Anti-ferromagnetism modifies periodicity
Resonant scattering can measure long range spin order

## Slide 38: Measuring Antiferromagnetic Dynamics
Intensity
Absorption
Diffraction
La1.5Sr0.5MnO4 (¼, ¼, ½) magnetic peak

## Slide 39: Measuring Antiferromagnetic Dynamics
Intensity
Absorption
Diffraction
La1.5Sr0.5MnO4 (¼, ¼, ½) magnetic peak
H. Ehrke et al. PRL 106, 217401 (2011)
70 ps experimental resolution

## Slide 40: Measuring Antiferromagnetic Dynamics
Intensity
Absorption
Diffraction
La1.5Sr0.5MnO4 (¼, ¼, ½) magnetic peak
LCLS measurements
300 fs (experiment limited) + 1.8 ps (diffusion?)
Phonons?

## Slide 41: Measuring Antiferromagnetic Dynamics
Completely suppress magnetic order in ~300 fs
Sr2IrO4
M Dean et al. Nature Materials 15 601 (2016)
Ir edge 11 keV

## Slide 42: Measuring Antiferromagnetic Dynamics
Sr2IrO4
M Dean et al. Nature Materials 15 601 (2016)
Ir edge 11 keV
Resonant Inelastic X-ray Scattering (RIXS)
Measure energy and momentum of scattered photons
Short-range spin correlations are unperturbed by photoexcitation
Phonons excited by pump pulse
Phonons responsible for demagnetization?

## Slide 43: Nanoscale femtosecond dynamics
Liu et al. Physical Review B 91 245155 (2015)
How can we image the role of spatial inhomogeneity on the dynamics?

## Slide 44: Holographic imaging
75 nm thick VO2 (PLD)
100 nm Si3N4 (amorphous)
1 μm Au
Field and intensity in the far field
Fourier transform of the recorded signal
Auto correlation at centre of FT
Cross correlation offset by d

## Slide 45: Holographic imaging
3 reference holes to increase S/N

## Slide 46: Holographic imaging
Advantages
Aberration free
Easy working environment
Stable to vibrations
Image in a “single shot”

## Slide 47: Imaging phase transitions statically

## Slide 48: Towards femtosecond dynamics
Laser induced damage!
X-ray induced damage!

## Slide 49: Conclusions
Ultrafast physics can disentangle and probe the interaction of multiple degrees of freedom
A range of techniques are required to understand the process that occur on the femtosecond timescale
Ge2Sb2Te5 – Fast thermal transition via intermediate liquid state
VO2 – Ultrafast structural transition suggesting dominate electron-phonon coupling
Manganites and irridates – Demagnetization of AFMs can be very fast, is non-equilibrium spin lattice coupling the key?
First steps to nanoscale femtosecond dynamics via X-ray holography

## Slide 50: Funding

## Slide 51: Cr2O3
Room temperature anti-ferromagnet insulator (TN=308 K)
100 % doped version of Ruby (Al2O3:Cr), same structure as V2O3
Centro-symmetric above TN.
Magnetic symmetry breaks time and space inversion.
EE
EE

## Slide 52: Magnetic Second Harmonic Generation
Polarizer
Colour Filter
Fundamental
Cr2O3
V Sala et al. PRB 94 014430 (2016)

## Slide 53: Optical Measurement of Demagnetization
Pump with 3 photon energies
Quick drop in SHG signal (< 70 fs)
Rapid recovery – wavelength dependent 400 fs at 1.8 eV, 300 fs at 3 eV
Long lived state >> 400 ps
Can we interpret this as magnetic dynamics?
V Sala et al. PRB 94 014430 (2016)

## Slide 54: Optical Measurement of Demagnetization
V Sala et al. PRB 94 014430 (2016)
t = 2 ps
System has demagnetized by Δl/l = 0.75%
Independent of pump wavelength

## Slide 55: Polarization Dependence
Early response is not magnetic
Dependent on pump wavelength
t = 0 ps

## Slide 56: Phonon Response?
M. Fiebig PRL 73, 2127 (1991)
SHG process is resonantly enhanced
Resonance enhanced by the crystal field
Crystal field perturbed by phonon modes
Cr2O3 supports Ag and Eg vibrations
High frequency results in incoherent excitation

## Slide 57: Ag Mode
Mode preserves symmetry
3 eV pump

## Slide 58: Eg Mode
1.8 eV pump
Mode breaks symmetry

## Slide 59: Cr2O3 magnetization dynamics
Phonons drive demagnetization in Cr2O3
Demagnetization rate depends on phonon mode
Eg ~400 fs, Ag ~ 300 fs
Timescales consistent with manganites and irridates
V Sala et al. PRB 94 014430 (2016)
A1g phonon decay
Magnetisation