## Slide 1: Magnet design for revised SPring-8-II lattice
Shinichi Matsubara
on behalf of Magnet team
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023

## Slide 2: Milestone of SPring-8
XFEL, "SACLA"
SR facility
"SPring-8"
Beam injection
2014: SPring-8-II CDR
2019~: Construction start of a 3 GeV light source, NanoTerasu in Japan
    Design and developments for SPring-8-II have been extensively applied, except for permanent magnets.
2022~: Design restart of SPring-8-II
2020: Beam injection from the SACLA linac
to the storage ring of SPring-8
  Shutdown old injector
  → Reduction of power consumption
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023

## Slide 3: Revised parameters of SPring-8-II
 | SPring-8-II |  | SPring-8
 | Revised design | Previous design (CDR in 2014) | 
Energy [GeV] | 6 |  | 8
Stored current [mA] | 200 | 100 | 100
Circumference [m] | 1435.43 |  | 1435.95
Effect. Emittance [nm rad] | 0.111 0.05 w/DWs | 0.15 | 2.7
Five-bend achromat lattice
Four longitudinal Gradient Bends (LGB) and a normal bend magnets
DQ-combined function magnets
Extra damping by damping wigglers in addition to undulators
Energy savings
SPring-8-II
achromat optics
New!
New!
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023

## Slide 4: Magnet configuration of a unit cell
← Beam
Name |  | #/normal cell | Type
Dipole | Normal | 1 | Permanent magnet
Normal Bend | Four segmented LGB | 4 | 
DQ-combined function | DQ Combined function | 4 | To be decided soon
Quadrupole |  | 16 | Electromagnet
Sextupole |  | 10 | 
Octupole |  | 4 | 
DQ
DQ
LGB
LGB
NB
DQ
LGB
DQ
LGB
B1
B2
B3
B4
B5
44 unit-cells + 4 long-straight-cells
Configuration of magnets for a unit cell
(Five-bend achromat lattice)
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023

## Slide 5: Magnet list
Name |  | #/normal cell | Total # | Max. field | Gap/ Bore dia. [mm]
Dipole | Normal | 1 | 44 | 0.953 [T] | 25
 | LGB | 4 | 176 | 0.615 [T] | 25
 | DQ-combined function | 4 | 176 | 0.259 [T] 23.8 [T/m] | 56
Quadrupole |  | 16 | 704 | 53.9 [T/m] | 34
Sextupole |  | 10 | 440 | 2,693 [T/m2] | 42
Octupole |  | 4 | 176 | 80,000 [T/m3] | 50
Dipole | DC septum | - | 2 | 1.4 [T] | 10
Dipole | Pulse septum | - | 1 | 1.4 [T] | 4
Injection part
PM
EM
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023

## Slide 6: Design strategy of permanent magnet
Radiation durability
  Sm2Co17 permanent magnet after proper annealing
  Permeance coefficient as large as reasonably possible
Compensation of temperature dependence
  Magnetic shunt with Fe-Ni temperature compensation alloy
  Pole gap field temperature dependence < ±5×10-5 /K
  The target range is comparable to the stability of electromagnets.
Magnetic field adjustment
  Tunable magnetic shunt with movable iron plates
  Correction for individual fabrication errors and long-term demagnetization
Field monitoring for demagnetization
  Observation slot in the return yoke for measuring the magnetic field strength correlated to the pole gap field
  High-precision NMR probe
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023

## Slide 7: Radiation damage tests: Nd vs SmCo
Blue: Sm2Co17 without annealing
Red: Nd-Fe-B with annealing [*]
Bizen and their team measured the radiation damage for Nd-Fe-B magnet.
In their setup, 8 GeV electron bunches hit magnet for hours.
The same experimental setup for SmCo
A magnet with annealing is known to be less demagnetized.
Measured radiation damage was quite different.
[*] T.Bizen et al., NIMA 574 (2007) 401.
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023

## Slide 8: Two major manufacturers of Sm2Co17 in Japan
Manufacturer | TOKIN, LM-32SH |  | ShinEtsu, R32HS | 
Model name | Specification | Measured | Specification | Measured
Remanence Br [T] | 1.12 ~ 1.20 | 1.16 1.17 1.17 | 1.10 ~ 1.18 | 1.12 1.12 1.12
Coercivity HcJ [kA/m] | > 1,592 | 1,729 1,990 2,210 | > 1,751 | 1,881 1,898 1,922
Maximum Energy Product (BH)max [kJ/m3] | 223 ~ 256 | 251 251 256 | 223 ~ 263 | 232 233 235
Thermal coefficient [/K] | -4 x 10-4 |  | -4 x 10-4 | 
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023

## Slide 9: Temperature distribution
Four long straight cells:
Few magnets in the long straight cells
RF cavity
Temperature distribution inside the current SPring-8 storage-ring
Position in the storage-ring
Difference of 3 K
The temperature changes depending on positions and time.
Shutdown period
Long straight cell
Difference of 2.5 K
1 month
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023
Notes: 2, 14, 26, 38cell

## Slide 10: Normal bend magnet
Sm2Co17 (TOKIN, LM-32SH)
Magnetic flux density :0.95 T
  (SPring-8-II bend magnet maximum)
Adjustment range : >10%
Magnet shape: large permeance coefficient
Pc (3 ~ 5)
BL = 0.95T x 0.4m
14%
Prototype
Outer plate for magnetic field adjustment
Magnetic shunt alloy
Gap-ﬁeld strength variation
Position of outer plate [mm]
0 50 100 150 200 250
1.12
1.10
1.08
1.06
1.04
1.02
1.00
0.98
0.96
0.94
B [T]
Iron
Sm2Co17
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023

## Slide 11: Design of LGB magnet
Longitudinal position Z [mm]
By [T]
LGB-B1
a
b
c
d
Smooth field transition between segments without field drops
a
b
c
d
e-
Same gaps for all segments to avoid complicated field distribution and minimizing PM volumes.
Nose structure
Shunt plate (iron)
PM: Sm2Co17
Nose structure
Spacing between segments
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023
Longitudinal axis Z
Prototype

## Slide 12: DQ-combined function magnet
Shunt alloy (Fe-Ni)
PM (Sm2Co17)
Beam axis
x= ~10 mm
Adjustment bolts
B = 0.259 T
B’ = -22.8 T/m
（B’/B = 88.0[m-1] ）
B’L = 7.98 T
Leff = 0.35 m
Quadrupole shape
Field adjustment
Splitable in half
The arrangement of two permanent magnets is simple and less prone to multipole errors.
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023

## Slide 13: Magnetic field adjustment
・ 2% magnetic field adjustment
・ The target individual difference :
< ±0.2%.
・Magnetic field adjustment with adjustment bolts
Evacuation of bolts
Full-insertion of bolts
Adjustment bolts
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023

## Slide 14: Magnetic force for splitting
Opening about 30 mm by using side-screws
before lifting with a crane.
The load was 2.8 kN at splitted distance of 30 mm.
The weight of the lifted half body is 180 kg.
Magnetic force for splitting with simulation
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023
Side-screw →
Guide bolt

## Slide 15: Field gradient stability with splitting
← Measured at the factory
↑
Measured in the SPring-8 site
Slight decrease of B’ was observed at the first to third splitting.
After repeated splitting, B’ became constant within 0.1%.
We think the decrease of B’ is related to the hysteresis. We will investigate it.
Different Hall sensor
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023

## Slide 16: DC septum magnet
[*] T. Taniuchi et at., Phys. Rev. Accel. Beams 23, (2020) 012401.
Minimize the leakage magnetic field
Additional PMs
for canceling out the field out of septum
Large Pc for prevention of demagnetization
Additional PMs
7 mm thick
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023
B = 1.4 T
Pole gap : 10 mm
Pole length : 0.4 m

## Slide 17: DC septum magnet
Lower shunt plate
upper shunt plate
Inserted NMR probe
Field monitoring slot
The gap ﬁeld strength can be varied by moving the shunt plates inside the return yoke.
Variable ranges : 4%
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023
Notes: DCseptum_20191211.pdf

## Slide 18: 3-year operation at the ring injection
4 segments（Nd×2, SmCo×2）
B = 1.1 T, BL = 2.3 T・m
Gap length 17 mm
Beam
Seg.1
Seg.2
Seg.3
Seg.4
Segment | Seg.1 (SmCo) | Seg.2 (Nd) | Seg.3 (SmCo) | Seg.4 (Nd)
Demagnetization ratio | -0.48% | -0.03% | -0.02% | -0.05%
PM-based bend magnet had been operated at injection part in 2018-2021.
For the 3 years, there was commissioning of the beam injection from SACLA with a significant beam loss of tens of %.
Significant demagnetization was observed only in the most upstream segment.
~5,000 Gy
All PMs were not annealed.
Storage ring
Beam
PM-based
bend magnet →
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023

## Slide 19: Closing
Design of SPring-8-II restarted.
Detailed design of the magnets are in progress for the revised SPring-8-II lattice.
We will prepare revised prototype magnets in 2024.
Procurement of components will begin in 2025.
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023

## Slide 20: SPring-8-II schedule (planned)
FY2023 | FY2024 | FY2025 | FY2026 | FY2027 | FY2028
Shutdown
SPring-8 user operation
Lattice optimization
NanoTerasu
Prototype
Procurement
Fabrication/Assembly/Test/Tuning…
Design,
Fabrication,
Test
Acc removal
Construction
Commissioning
Hardware design
Here
Design revision
3 GeV Ring
Low Emittance Ring - Permanent Magnets Workshop -TRIESTE, Nov 14-15, 2023