## Slide 1
Update on measurement and operation of a ZEPTO tunable permanent magnet quadrupole on Diamond Light Source
Alex Bainbridge
ASTeC, UKRI-STFC Daresbury Laboratory
Low Emittance Ring – Permanent Magnets Workshop
14-15 November 2023
Trieste, Italy

## Slide 2
1 Introduction to ZEPTO
Development and motivation of ZEPTO tuneable permanent magnet technology.
2 Magnet assembly
Challenges of assembling a tuneable permanent magnet with strong forces present.
3 Lab measurement results
Gradients and compensation of magnetic centre movements.
5 Beam based measurements and operations to date.
Agenda
4 Installation on Diamond
Gradients and compensation magnetic centre movements.

## Slide 3
The original motivation- CLIC
333 dipoles
333 dipoles
42000 quadrupoles
288 dipoles
288 dipoles
ZEPTO (Zero Power Tuneable Optics) project started as a collaboration between CLIC (Compact Linear Collider) and STFC Daresbury Laboratory.
Aim is to save power and costs (both financial and environmental) by switching from resistive electromagnets to permanent magnets.

## Slide 4
The ZEPTO project created 3 prototypes for CLIC.
All were designed, constructed and measured at STFC Daresbury Laboratory.
All use NdFeB magnet blocks attached to a motion system, with fixed steel poles defining the field shape.
Project 1: High strength quad
B gradient from 60 – 15 T/m
Shepherd et al, Journal of Instrumentation, Vol 9, T11006, 2014
Project 2: Low strength quad
B gradient from 43 – 3.5 T/m
Shepherd et al, IPAC’14, Dresden, Germany, paper TUPRO113.
Project 3: Wide range dipole
B adjustable from 1.1 T to 0.45 T
Bainbridge et al., IPAC’17, Copenhagen, Denmark,, paper THPIK105.
Zero Power Tuneable Optics (ZEPTO)
2017-2019
2012 - 2014

## Slide 5
New technology demonstrator
We want to show that the benefits of ZEPTO technology are not limited to CLIC, and can be used as an energy saving `drop-in' replacement for electromagnets on accelerators such as existing light sources.
So we developed a new ZEPTO quadrupole for the booster-to-storage ring section of Diamond Light Source.
0
0.2
0.4
1.2
0.8
1.0
0.6
1.4
0.2
0.4
1.2
0.8
1.0
0.6
1.4
Contours B (T)

## Slide 6
OPERA 3D model
SmCo blocks attached to vertical motion system with 90mm movement range and 1 µm precision
Fixed “inner yoke” defines the quadrupole field
Fixed “outer yoke” can steer flux away from the beam, allowing the gradient to be adjusted
No magnetic contact between yokes, the gap between is filled with aluminium for rigidity
Simulations predicted a gradient tuning range from 23 T/m down to 0.35 T/m
The outer yoke acts as a short circuit for the flux, allowing the magnet to be ‘turned off’.
New technology demonstrator
32 mm aperture

## Slide 7
Previous ZEPTO magnets used large NdFeB blocks to produce the magnetic flux, which are difficult to manufacture and handle.
New magnet uses a “carriage” with a number of smaller blocks set into an aluminium latticework.
Advantages over larger single blocks which include:
Blocks are easier and cheaper to manufacture.
Damaged single blocks may be replaced instead of the entire carriage.
Variation in block BH curves may be compensated.
Modular magnet "families" may be created by strategic removal of blocks.
The gaps between blocks do not affect field quality as the flux must pass through a steel pole before reaching the beam.
We use SmCo instead of NdFeB for improved radiation hardness and temperature stability.
No thermal shunts are needed
Permanent magnets
300 mm
33 mm
50 mm

## Slide 8
In previous ZEPTO quadrupoles field measurements revealed the magnetic centre moving as function of magnet block position, mostly vertically, due to unexpectedly magnetic components.
Expecting this, each magnet carriage now has a dedicated motor and associated driving ball screw to help compensate.
Look-up table can be applied to either carriage position to compensate and restore the magnetic centre to the geometric centre.
Dual motor system
Shepherd et al, IPAC’14, Dresden, Germany, paper TUPRO113.
Motor
PM Carriage
Ball screw
Carriage holder

## Slide 9
Split design
Electromagnetic quadrupoles can typically be split for installation around an existing vacuum vessel – previous ZEPTO quadrupoles could not.
The new version may be split about the vertical axis and reassembled around an existing vacuum system using a dedicated assembly frame.
This allows replacements or repair to be conducted without needing to keep the accelerator offline for the additional time needed to restore the quality of the vacuum.
Vacuum chamber
Temporary PM carriage holder
Pre-bolted inner and outer yokes
Yoke supports
Rail

## Slide 10
Split design
Electromagnetic quadrupoles can typically be split for installation around an existing vacuum vessel – previous ZEPTO quadrupoles could not.
The new version may be split about the vertical axis and reassembled around an existing vacuum system using a dedicated assembly frame.
This allows replacements or repair to be conducted without needing to keep the accelerator offline for the additional time needed to restore the quality of the vacuum.

## Slide 11
Construction
To ensure that the inner yoke structure is properly positioned, both yokes were pre-assembled with Aluminium spacers before final machining.
Wire erosion used to achieve <30 µm precision on pole tips, regardless of tolerances of initial manufacture.
Dowel system should ensure repeatability of assembly
300 mm
400 mm

## Slide 12
Assembly forces
Simulated
Estimated
Extrapolated
Forces between the PM blocks and steel yokes must be calculated in advance and managed during assembly!
A Hall probe was used to measure the flux density entering the steel yoke for as much of the approach as possible, and from this an estimate of the actual force was derived

## Slide 13
Operational forces
FX
FY
The simulated magnetic forces are a function of PM block position and are highly complex
Horizontal forces are balanced on each side of carriages but act on the steel yoke, causing a movement risk to components.
FX
FY

## Slide 14
Gradient vs gap
Some variation between simulated and measured gradients observed.
Gradient lower than predicted but still within requirements (19 to 0.5 T/m normal operation)
Actual range of sweep is 1-85 mm (instead of 0-90 mm) due to limit switch positions.
Tuneability 22.37 to 0.47 T/m
Predicted range was 22.72 T/m to 0.3 T/m

## Slide 15
Vertical centre position
Movements in Y centre observed as a function of carriage position.
Y centre slowly rises as gap enlarges and then suddenly starts to drop.
Cause of movement and direction reversal unknown – magnetic materials in pedestal? Uneven motion?

## Slide 16
Vertical centre position
By offsetting the bottom carriage position from the top carriage position we have found this is correctable!
Works with either carriage, but resulting look-up table is slightly different.

## Slide 17
Vertical centre position
By applying the look-up table we can effectively counter all vertical movement of the magnetic centre!
Dataset shown has 7 µm drop in centre position, with 5 µm drop expected from temperature variation alone (contraction of magnet pedestal).

## Slide 18
Horizontal centre position
Movements in X centre also observed as a function of carriage position.
This is more of a problem – cannot be countered by offsetting magnet carriages!
Further concerns about the repeatability of the position – are parts sticking/slipping with changes to magnetic forces?

## Slide 19
Horizontal centre position – one explanation
Can replicate trend by offsetting one half of outer yoke – Assembly issue?

## Slide 20
Harmonic measurements
Harmonics were measured by moving the Hall probe in a circular pattern at several positions along the length of the magnet.
Harmonics are reasonably consistent with PM carriage position.
The octupole harmonic is expected in this case due to the loss of a symmetry axis.

## Slide 21
Installation on Diamond
The magnet was installed on the Diamond BTS line in August 2022.
It is located 1.5m downstream form an EM quad that has now been switched off.
The installation was done without breaking the vacuum, something that would have been impossible with previous designs.

## Slide 22
Installation on Diamond
The magnet was installed on the Diamond BTS line in August 2022.
It is located 1.5m downstream form an EM quad that has now been switched off.
The installation was done without breaking the vacuum, something that would have been impossible with previous designs.

## Slide 23
Installation on Diamond
The magnet was installed on the Diamond BTS line in August 2022.
It is located 1.5m downstream from an EM quad that has now been switched off.
The installation was done without breaking the vacuum, something that would have been impossible with previous designs.

## Slide 24
Restoring injection
ZEPTO is 1.5 m downstream of the magnet it replaces, some disruption to the lattice is unavoidable. The ZEPTO gradient can be reduced to <0.5 T/m, but not to true zero field.
New lattice settings minimised the differences. The beta functions are well corrected, with only some minor differences around the ZEPTO magnet.
Injection efficiency ~70% both before and after installation (actually slightly better after….)

## Slide 25
Beam based gradient measurements
Beam based measurements were used to check gradient in X and Y planes. (upstream corrector adjusted to offset through magnet and resulting kick measured)
Although this method is somewhat crude, the Horizontal plane shows good agreement with Lab based measurements, though ~0.6 T/m higher.
The vertical plane agrees less well, but the same issue was seen attempting to do the same with the electromagnet – suggests sensitivity of BTS to vertical changes rather than ZEPTO issue.

## Slide 26
Beam based magnetic axis measurements
Beam-based measurements of the magnetic axis position of ZEPTO checked at axis movement against gradient.
Results show that any changes in axis position as the gradient is adjusted are small and unlikely to cause adverse effects.
These measurements use the lookup table developed in lab measurements to correct vertical movement of the axis.

## Slide 27
Current status
Magnet is currently still operating on the BTS line replacing the electromagnetic quad, and saving 136 kg of CO2 per year.
The radiation dose being received is being measured by a moderated TLD to detect neutrons and 4 TLDs that monitor γ radiation.
Between 8th Feb and 25th July accumulated doses were 25 mSv of neutron and 22 Sv of γ on the highest reading TLD (11 Sv on next highest)
The magnet was briefly set to minimum and EM turned back on to investigate motor stalls, turned out to be an issue with the control system!

## Slide 28
We have built a new ZEPTO quadrupole prototype with several evolutions over the original prototypes.
We have successfully demonstrated that it is possible to build a ZEPTO magnet that can be split and installed around an existing beam pipe.
We have shown that it is possible to keep the vertical magnetic centre position stable by individually moving the magnet blocks according to a look-up table.
The magnet has been successfully installed and operated on the BTS line of Diamond Light Source.
Its still going a year later and appears to have survived in the environment for a year. Paper in preparation….
Conclusions

## Slide 29: Acknowledgements
The team behind ZEPTO DLS prototype:
Ben Shepherd
+ Thanks to Alex Headspith, Callum Otter, Ryan Cash, Mike Liptrot, Paul Hindley and Mike Lowe
Alex Bainbridge
Nick Krumpa
  This work was funded by the STFC Proof of Concept Fund
Alex Hinton
Group Leader & ZEPTO co-inventor
Design & Modelling
Mechanical engineering
Measurements
Ian Martin
Diamond AP Leader
Beam based measurements
Rick Fielder
Walter Tizzano
Diamond project lead

## Slide 30
Thank You
@STFC_matters
Science and Technology Facilities Council
Science and Technology Facilities Council