## Slide 1
Ed Rial on behalf of HZB Undulator Group, 29. November, 2019
European Synchrotron Light Source Workshop 2019, Barcelona
Undulator Developments at HZB

## Slide 2: Undulator Developments at HZB
Contents
Background
CPMU17
IVUE32
Cryo-UE15
Future ideas and challenges
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
OPPORTUNITIES

## Slide 3: Experience of BESSY
1998
1999
1999
1998
1999
2000
2000
2001
2002
2002
2003
2004
2004
2006
2007
2007
2009
2010
2015
2017
U49-1
U125-1
UE56-1
UE56-2
U41
U49-2
U125-2
UE56
UE46
UE52
UE56 R
U139
UE49
UE112
U48
UE56 K
UE65
CPMU9
UE48
CPMU17
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
U49-1
UE56-2
UE56-1
U41
U49-2
U125-2
UE46
UE52
U139
UE49
UE112
UE48
CPMU17

## Slide 4
High Flux
High Brightness
High Energy
Large Energy Range
  Constant Flux!
  No Energy Gap!
Fully Polarisable
  Pure polarised light only please!
  Fast switching!
High Flux
High Brightness
High Energy
  CPMU
Large Energy Range
  Multi-lu Undulators
Fully Polarisable
  APPLE Undulators
Fast Switching
  TRIBs
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
High Flux
High Brightness
High Energy
Large Energy Range
  Constant Flux!
  No Energy Gap!
Fully Polarisable
  Pure polarised light only please!
  Fast switching!
User Requirements
Notes: Chopper 100Hz – TRIBS 1MHz

## Slide 5
CPMU
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
Development Path: CPMU

## Slide 6
A wide energy range for EMIL,
Energy Materials In-situ Laboratory
60 – 6000eV
Canted Double Undulator System
.
Dipole
Dipole
Dipole
CPMU17
UE48
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
CPMU17: EMIL @ BESSY

## Slide 7
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
CPMU17: Internal View

## Slide 8
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
CPMU17: Measurement System

## Slide 9
room temperature
liquid nitrogen
temperature
with taper correction
4° phase error
no taper correction
7° phase error
Final taper setting and environmental field compensation with monochromator
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
CPMU17: Measurement Results

## Slide 10
U17-DCM commissioning
Si 422 crystal
Si 111 crystal
Si 111 crystal
3rd Harmonic
5th Harmonic
7th Harmonic
CPMU17: Initial Spectral Results
Courtesy of F. Schäfers
Notes: V2C XES – valence to core emission spectroscopy
Analysis of the weak VtC XES region can be used for ligand identity around an absorbing atom. Main advantage over EXAFS: C, N, and O, may be distinguished by VtC XES. Moreover, information about metalligand bond lengths and the activation of diatomic ligands (CO, N2, O2, or NO) may also be extracted from analysis of VtC spectra.
Comparison of measurements done at PETRA III P64 beamline and at PINK, measurement time is the same

## Slide 11
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
CPMU17: Internal View

## Slide 12
CPMU17
Optical micrometer consisting of
transmitter, receiver, blades
Temperature dependent length variations
are compensated automatically
systematic optical errors of window flange are reproducible, can be corrected
Gap Reproducibility on 1 𝝁𝒎 –Level;
Well suited for cryogenic undulators
Hallprobe
bench
transmitter
receiver
window
window
aperture
J. Bahrdt, C. Kuhn, Synch. Radiation News Vo. 28 No 3 (2015) 9-14.
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
CPMU17: Gap Feedback
Notes: Cross section of the CPMU17, left: undulator, right: in-vacuum hallprobe bench
We need temperature independent gap measurement system
Systematic errors due to window quality, but: reproducible

## Slide 13
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
the importance of active gap feedback
CPMU17: Gap Feedback

## Slide 14
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
CPMU17: After One Year

## Slide 15
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
CPMU17: 2019 Modifications

## Slide 16
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
CPMU17: 2019 Modifications

## Slide 17
Nominal operation conditions.
Temperatures measured with PT100 thermocouples.
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
CPMU17: Heat Load in Operation

## Slide 18
CPMU
In-Vacuum APPLE
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
Development Path: In-Vacuum APPLE-II

## Slide 19
Interests at straight L06
Substitution of the U41 Undulator:
METRIX and PEAXIS need:
  vertical polarization
  no complicated directional characteristics
  Energy range: 250 - 1000 eV
Microscopy needs variable linear polarization
  no need to rotate sample rotation necessary
  (very problematic with microscopy)
Energy range: 250 - 2500 eV
  Beamline optimized for high energies
Additionally variable elliptic polarization over the entire energy range
APPLE II, elliptical mode
Room Temperature In-Vacuum UE32 | 
Period Length | 32 mm
Total Length | 2.5 m
Number of Periods | 78
Physical Aperture over 2.5m | 6.3 mm
Magnetic Gap | 7 mm
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
IVUE32: Requirements

## Slide 20
Comparison BESSY II-UE49
Increase in Brilliance and Flux >/= Factor 2
No gap in the spectrum in vertical linear polarisation
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
IVUE32: Spectral Performance

## Slide 21
Functional Magnets (FMs) at the center Compensation Magnets (CMs) at the sides and top / bottom
Source: Bahrdt, Johannes & Grimmer, In-vacuum APPLE II undulator with force compensation. AIP Conference Proceedings. 2054. 030031. 10.1063/1.5084594.
Staggered column design
Magnetic force Compensation
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
IVUE32: Mechanical Design Aspects

## Slide 22
Polarization modes:
Elliptical (solid)
Inclined (dashed)
Uncompensated
Small CMs
Large CMs
Gap = 40mm
Gap = 7mm
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
IVUE32: Magnetic Design Aspects

## Slide 23
IVUE32 Design work in progress
Development of magnet soldering technique on-going
Keeper design including force compensation magnets
Optimization of cast iron frame with casting company
Implementation of transverse column adjustment
Reduction of column height and bellow diameter
Finalization of gap drive mechanism
10 period prototype designed and ordered
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
IVUE32: Status

## Slide 24
In-Vacuum APPLE
CPMU
Cryo-APPLE
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
Development Path: Cryogenic APPLE

## Slide 25
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
Traditional APPLE II
Modified APPLE II
Horizontal Polarisation
Vertical Polarisation
2mm Gap : 15mm Period: 15x15mm Block : PrNdFeB @77K
CUE-15: Magnetic Design

## Slide 26
Short Period Cryogenic Undulator
A fully tested, operational cryogenic undulator adapted to the ATHENA needs (to be installed at ATHENAe); financed by budget applied for by DESY as part of the ATHENA proposal.
Polarisation
Peak Field (T)
K
H
1.91
2.67
V
1.36
1.91
C
1.13
2.25
Potential Solution – First Look
In-Vacuum Cryogenic APPLE device
λu = 15mm
Minimum Gap = 2mm
Block cross section 15mm x 15mm
Replicate Force-Compensation Design
Designed using Pr-NdFeB magnet material near 77K
Can match K-Value of 2.11 of existing device (FROSTY)
Variable Polarisation
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
CUE-15: Magnetic Summary

## Slide 27
CPMU
In-Vacuum APPLE
Multi-lu
Undulator
Cryo-APPLE
Cryo-Multi-lu
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
Development Path: Cryo Multi Period

## Slide 28
20mm
BESSYII
  Low-Energy X-ray Specialists…
  …with designs on tender X-Ray regime.
Easier technologically than Cryo-APPLE
Development depends on user demand
TRIBs?
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
CryoMlU: Concept

## Slide 29
CPMU
In-Vacuum APPLE
Multi-lu
Undulator
Cryo-APPLE
Cryo-Multi-lu
IV
Multi-lu
APPLE
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
Development Path: IV Multi Period APPLE

## Slide 30
Polarisation Switching
  Mechanical Chopper ~ 100Hz
  TRIBs ~1MHz
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
CryoMlA: Concept

## Slide 31
CPMU
In-Vacuum APPLE
Multi-lu
Undulator
Cryo-APPLE
Cryo-Multi-lu
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
Development Path:
Development Path: Moon-on-a-stick
IV
Multi-lu
APPLE

## Slide 32
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
US-X
US-Y
US-Z
Triple Period Undulator:
Vacuum chamber
Front
Above
Small-Gap Cryogenic-APPLE TPU
Vision: Extend the photon energy range provided by IDs and provide continuously high flux across the energy range.
Building on current knowledge to exploit future possibilities made available by next generation synchrotron light sources, and provide users with their moon – on a stick!
Triple Period Cryo APPLE: Motivation
Moon-on-a-stick: Motivation
Challenge
OPPORTUNITY

## Slide 33
The Undulator Team at HZB
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
Johannes Bahrdt, Atoosa Meseck, Jürgen Bakos, Winfried Frentrup, Stefan Gottschlich, Stefan Grimmer, Maryam Huck, Carsten Kuhn, Florian Laube, Christoph Rethfeld, Anette Rogosch-Opolka , Michael Scheer, Bodo Schulz.
Specifically J. Bahrdt & A. Meseck
Special thanks to Franz Schäfers
Acknowledgements

## Slide 34: U125-2
timeline
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019
U125-2

## Slide 35: UE56-2
UE56-2

## Slide 36: U41
U41

## Slide 37: U49-1

## Slide 38: UE49
UE49

## Slide 39: UE52
UE52

## Slide 40: UE46
UE46

## Slide 41: U139
U139

## Slide 42: UE56-1
UE56-1

## Slide 43: CPMU17
CPMU17

## Slide 44: UE48
UE48

## Slide 45: UE112
UE112

## Slide 46: U49-2
U49-2

## Slide 47: Experience of BESSY
1998
1999
1999
1998
1999
2000
2000
2001
2002
2002
2003
2004
2004
2006
2007
2007
2009
2010
2015
2017
U49-1
U125-1
UE56-1
UE56-2
U41
U49-2
U125-2
UE56
UE46
UE52
UE56 R
U139
UE49
UE112
U48
UE56 K
UE65
CPMU9
UE48
CPMU17
E. Rial, Undulator Developments at HZB, 29.11.19
European Synchrotron Light Sources 2019