## Slide 1
Alexandre Ponrouch
Lifting the veil on the passivation layers in
Ca and Mg-metal anode based batteries:
A complementary FTIR (MIRAS) and
XPS (CIRCE) spectroscopies study
INSTITUT DE CIÈNCIA DE MATERIALS DE BARCELONA
ALBA-ICMAB
Workshop
February 24th

## Slide 2: Beyond Li based technologies
high energy density, low cost and safety (dendrite)
Li+/Li
Ca2+/Ca
Mg2+/Mg
-3.04
-2.87
Na+/Na
-2.71
-2.37
Chart: 
| Li | C | Na | Mg | Ca
 | 2080 | 500 | 1120 | 3800 | 2060
 | 3860 | 372 | 1160 | 2000 | 1340
Dendrite
(Li-ion)
Volumetric
(mAh/cm3)
Gravimetric
(mAh/g)
Capacity
Voltage
NHE
E ˚
0
(…)
Abundance in crustal rocks (ppm)
Cost of raw material ($/ton)
Chart: 
| Li | Na | Mg | Ca
cost of raw material ($/ton) | 1 | 1 | 1 | 1
Abundance | 2 | 2 | 2 | 2
Li Na Mg Ca
5000
Li Na Mg Ca
Chart: 
| Li | Na | Mg | Ca
Abundance in crustal rocks (ppm) | 1 | 1 | 1 | 1
50000

## Slide 3: Interface and interphase
Interface
Passivation layer ?
Ca
or
Mg

## Slide 4: Multivalent Challenges
Passivation
Electrolyte
M = Mg, Ca
Mg2+
Ca2+
Focus on electrolytes in which
no passivation occurs
(ethereal solutions)
Reversible plating and stripping
thought to be impossible !
Mg
Ca
Lithium
Mg and Ca
Aurbach et al., J. Electrochem. Soc., (1991)

## Slide 5: Ca plating with passivation layer (SEI)
Ponrouch et al., Nat. Mater., 15 (2016) 169
RoomT
75˚C
100˚C
TOYOTA
After plating
After stripping
FTIR
Electrolyte stability > 4 V
100˚C; 0.2 mV/s

## Slide 6: BF4 vs TFSI based electrolytes
Why TFSI based electrolyte does not allow for Ca plating?

## Slide 7: BF4 vs TFSI based electrolytes
  Ca(TFSI)2
  Pristine Ni particle
  Ca(BF4)2
Ni particle
J. Forero
Saboya
J. Forero Saboya, I. Yousef et al., in preparation

## Slide 8: BF4 vs TFSI based electrolytes
  Ca(TFSI)2
  Pristine Ni particle
  Ca(BF4)2
Ni
Ni
Conformal passivation layers
Thinner film with TFSI
(yet fully blocking)
Ni particle
J. Forero Saboya, I. Yousef et al., in preparation

## Slide 9: SEI component allowing for Ca plating
C 1s
CO3
COO
C-O
CH2/CH3
B 1s
BxOy
J. Forero Saboya, I. Yousef et al., in preparation
FTIR
  Ca(TFSI)2
  Ca(BF4)2
Presence of borate
XPS

## Slide 10: BF4 vs TFSI based electrolytes
10
TFSI
vs.
BF4
Pre passivation in BF4 based electrolyte
Good passivation is mandatory
Electrolyte significantly impact the plating / stripping kinetics
J. Forero Saboya, I. Yousef et al., in preparation

## Slide 11: Preliminary work at MIRAS
J. Forero Saboya, I. Yousef et al., in preparation
FTIR-Microspectroscopy

## Slide 12: Perspectives
MIRAS (FTIR)
Beamtime in June (proposal 2019083680)
Electrolyte formulation => SEI composition and homogeneity
Investigation on standard borate samples
Far IR (<700 cm-1) study => cation coordination and ionic conductivity

## Slide 13: Perspectives
CIRCE (XPS)
Apply for beamtime
Complementary to FTIR
Perfect combination for the characterization of passivation layer in batteries
SEI
CIRCE (XPS)
MIRAS (FTIR)
Varying the photon energy (depth analysis)
Near ambient pressure photoemission (NAPP)

## Slide 14
THANK YOU FOR YOUR ATTENTION!

## Slide 15: Multivalent Challenges
Electrolyte electrochemical stability window (HOMO/LUMO)
Potential
Scale
(V vs M+/M)
Battery operation window
Kinetics limitation for electrolyte reduction
(SEI)
Kinetics limitation for electrolyte oxidation
(Surface layer)
Low voltage negative electrode
High voltage positive electrode
SEI and surface layer needed for high voltage
(high energy density)
0

## Slide 16: Interfaces and interphases
Electrochemical impedance spectroscopy: Ca//Ca symmetric cells
Influence of solvents
=> Power performances could be significantly enhanced!
Rct + desolvation energy + R SEI
Influence of additives
No additive
1% additive

## Slide 17: Binding energy and plating kinetics
Improving kinetics by tuning the solvation shell
TFSI (0.45M)
vs.
BF4 (0.45M)
Pre passivation in BF4 based electrolyte
No ion pair
Forero Saboya et al., J. Phys Chem. C accepted

## Slide 18: Ca plating
Substrate
SEI
Electrolyte
Ca2+ (Solvated)
①
②
Ca2+ (Desolvated)
③
Ca (Nucleation and growth)
④
① and ② Ca2+ diffusion/migration within the electrolyte and/or desolvation may be hindered
③ Ca2+ diffusion within the SEI may be hindered
④ Ca nucleation and growth may be hindered

## Slide 19: Ca plating !
Ponrouch et al., Nat. Mater., 15 (2016) 169
After plating
After stripping
Infrared and XPS of the calcium deposit
The SEI is stable upon cycling and fully covering!!!
Ca2+ cations seem to migrate through the SEI
Ca 2p
2p3/2
2p1/2
FTIR
XPS
Forero Saboya et al., in preparation
Ca 2p
2p3/2
2p1/2
XPS

## Slide 20: Solvation shell – Binding energy
Improving kinetics by tuning the solvation shell
Complex | Binding Energy (Eb) (kJ.mol-1)
[Ca(EC)]2+ | 380
[Ca(TFSI)]+ | 1162
[Mg(EC)]2+ | 544
[Mg(TFSI)]+ | 1442
Forero Saboya et al., J. Phys Chem. C accepted