## Slide 1
Boron cluster presence in new materials for their use in polymers, biopolymers and medicine
Prof. Dr. Clara Viñas i Teixidor
Inorganic Materials & Catalysis Laboratory
ALBA-ICMAB workshop
Alba synchrotron
February 24th 2020
T

## Slide 2
R. Williams,
1964
INTRODUCTION
Boron natural:
20% 10B
80% 11B

## Slide 3
Fullerene C60:
Vertices only a C
Carbon Compounds
T
INTRODUCTION

## Slide 4
Boron Compounds: boranes, carboranes
Vertices: B-H bond
R.W. Rudolph, W.R. Pretzer,
Inorg. Chem. 1972, 11, 1974.
INTRODUCTION

## Slide 5
INTRODUCTION
Neutral
dicarborane
Anionic metallabis(dicarborane)
M= Co3+, Fe3+
Icosahedral geometry
3D Aromatic Structure
Stable anions
Non-localized negative charge
Soluble in water or organic solvents depending on the cation
Photocatalysts

## Slide 6
What is Boron Neutron Capture Therapy?
10B 1n 7Li 4He
+
+
+  photon
C
C
C
C
C
C
10B
10B
10B
C
C
C
Selective labeling
with 10B
Capture of slow
neutron
Tissue repair
Requirements:
∼20 μg of 10B / g tumor
Boron compound should be into the cells: “radiolabeling”
Notes: But, what is Boron Neutron Capture Therapy?
BNCT is a bimodal cancer treatment based on the large neutron capture area of 10B nucleus. 10B captures slow neutrons core produces 7Li, a photon and α particle that can destroy cells (α particle has high kinetic energy, approximately 2.4 MeV).
The cancerous tissue, consisting of healthy and cancerous cells, is well irrigated so, tumor tissue gets more nutrients and more drugs. Irradiating the tissue with slow neutrons α particles are produced that can destroy cancer cells.
For the successful application of BNCT, a high concentration of boron should be delivered to the tumor cells. The amount of 10B needed for effective BNCT is more than 20 μg per gram of tumor.
Could these MNPs be suitable for BNCT radiation? It was prove that MNPs internalize cells and the amount of Boron 10 was of 26 20 μg per gram of tumor. It seems yes!!

## Slide 7
COSAN: on the road to anticancer therapies
Requirements of suitable boron delivery agents for the highest therapeutic and cost efficiency in BNCT are:
High selectivity for tumours
High uptake in tumours: ∼20 μg of 10B / g tumor
Low toxicity
Accumulating the boron within the nucleous of cancer cells
Notes: If COSAN accumulates within the nucleous, Does COSAN interact with DNS?

## Slide 8
INTRODUCTION
Neutral
dicarborane
Anionic metallabis(dicarborane)
M= Co3+ : CoSAN; Fe3+ : FeSAN
Icosahedral geometry
3D Aromatic Structure
Stable anions
Non-localized negative charge
Soluble in water or organic solvents depending on the cation

## Slide 9
Monolayer vesicles with polydisperse radius (aprox. 20 nm) and constant wall thickness (1.16 nm) in diluted water solution (1-13 mM).
Spherical micelles with of 1.16 nm radius and monolayer vesicles coexist at concentration higher than 13 mM.
Monolayer vesicles with polydisperse radius (80-890 nm) in saline solution.
P. Bauduin, S. Prevost, P. Farràs, F. Teixidor, O. Diat, T. Zemb, Angew. Chem. Int. Ed. 2011, 50, 5298 – 5300.
COSAN vesicles/micelles formation in water
B-H···H-Ccluster
M. J. Hardie and C. L. Raston, Chem. Commun., 2001, 26, 905
Notes: Our group reported in 2011 the unique property of the protonated salt of the cobaltabisdicarbollide to produce monolayer vesicles of about 20 nm of radius in diluted water solutions. When increasing the concentration, vesicles and micelles coexist. The radius of the vesicles increases to 80-890 nm in saline solution.
It is very important to emphasize that these vesicles are monolayer in contrast with liposomes and natural membranes that are bilayer.
Dihydrogen bond B-H ··· H-C are involved in both monolayers vesicles.

## Slide 10: Interaction between CoSAN vesicles and membranes?
vs

## Slide 11
C. Verdiá-Báguena, A. Alcaraz, V. M. Aguilella, A. M. Cioran, S. Tachikawa, H. Nakamura, F. Teixidor and C. Viñas, Chem. Commun., 2014, 50, 6700-6703.
Interaction between COSAN vesicles and membranes
First focus: “in vitro” interaction between lipidic membrane and CoSAN

## Slide 12
C. Verdiá-Báguena, A. Alcaraz, V. M. Aguilella, A. M. Cioran, S. Tachikawa, H. Nakamura, F. Teixidor and C. Viñas, Chem. Commun., 2014, 50, 6700-6703.
Visualisation of the interaction between COSAN vesicles and liposomes
CryoTEM
Images
Notes: Our aim was to prepare high Boron content MNPs to act as anticancer drug for dual therapy: Hyperthermia therapy (by the core composition) + BNCT (by the capping molecules).

## Slide 13
Alone cells
Cosan and
I2-Cosan solution
A
B
C
D
COSAN/Membranes interaction: Cell images
M. Tarrés, E. Canetta, C. Viñas, F. Teixidor, A.J. Harwood, Chem. Commun., 2014, 50, 3370-3372.
Notes: In 2011, we demonstrated that COSAN cluster crosses artificial bilayer organic membranes as well as cellular bilayer membranes.
We demonstrated that COSANE cluster accumulates into the cells and we visualized inside living cells by Raman Microscopy.

## Slide 14
COSAN: Membranes interaction
Accumulating / visualizing inside living cells
Crossing artificial membranes
Raman-Microscopy
C. Verdiá-Báguena, A. Alcaraz, V. M. Aguilella, A. M. Cioran, S. Tachikawa, H. Nakamura, F. Teixidor and C. Viñas, Chem. Commun., 2014, 50, 6700-6703.
M. Tarrés, E. Canetta, C. Viñas, F. Teixidor, A.J. Harwood, Chem. Commun., 2014, 50, 3370-3372
Notes: In 2011, we demonstrated that COSANE cluster crosses artificial bilayer organic membranes as well as cellular bilayer membranes.
We demonstrated that COSANE cluster accumulates into the cells and we visualized inside living cells by Raman Microscopy.

## Slide 15
COSAN: on the road to anticancer therapies
Optical microscopy images
Nanohybrid
CT-dsDNA
Na[CoSAN]
Second focus: “in vitro” interaction between ds-DNA with CoSAN
I. Fuentes, T. García-Mendiola, S. Sato, M. Pita, H. Nakamura, E. Lorenzo, F. Teixidor,. F. Marques, C. Viñas, Chem. Eur. J. 2018, 24, 17239–17254.

## Slide 16
BSA-Na[CoSAN]
0.6 nm
1.1 nm
100 COSANE
98 COSANE
COSAN: on the road to anticancer therapies
Third focus: interaction between CoSAN and protein (BSA)
I. Fuentes, J. Pujols, C. Viñas, S. Ventura, F. Teixidor, Chem. Eur. J. 2019, 25, 12820 – 12829.

## Slide 17
COSAN: “in vitro” cells study
M. Tarrés, E. Canetta, E. Paul, J. Forbes, K. Azzouni, F. Teixidor, C. Viñas, A.J. Harwood, Scientific Reports, 2015, 5, 7804
 | ED50 (mean ±SD, µM) | 
Cell type | COSAN | I2-COSAN
Mammalian cells |  | 
HEK 293 | 121 ± 3.8 | 30 ± 3.8
HeLa | 157 ± 8.6 | 23 ± 2.5
THP-1 | 154 ± 8.9 | 44 ± 6.0
3T3 | 99 ± 5.5 | 29 ± 0.8
Amoeba cells |  | 
D. discoideum | 2.6 ± 0.3 | 1.8 ± 0.1
Bacteria |  | 
E. coli B/r | > 250 | 53 ± 5.4
Klebsiella Kneumonia | > 250 | 65 ± 4.1
KK2 buffer: 6.5 mM KH2PO4, 3.8 mM K2HPO4, pH = 6.2
> 5 hours
COSAN is cytostatic
Notes: In 2015, we proved that COSAN is cytostatic stopping the cellular division and its effective doses 50 were calculated for several Mammalian, ameba and bacteria cells.

## Slide 18
CARBORANES: on the road to anticancer therapies
Gold nanoparticles
Magnetic nanoparticles (SPIONs)
E. Oleshkevich, A. Rosell, A. Morancho, K. Galenkamp, J. Comella F. Teixidor, C. Viñas, Nanomedicine: NBM, 2019, 20, 101986.
A. M. Cioran, A. D. Musteti, F. Teixidor, Ž. Krpetić, I. A. Prior, Q. He, C. J. Kiely, M. Brust, C. Viñas, J. Am. Chem. Soc., 2012, 134, 212.
Fe3O4/ γ-Fe2O3

## Slide 19
CARBORANES: on the road to anticancer therapies
Gold nanoparticles
Magnetic nanoparticles (SPIONs)
A172 glioblastoma cells
A. M. Cioran, A. D. Musteti, F. Teixidor, Ž. Krpetić, I. A. Prior, Q. He, C. J. Kiely, M. Brust, C. Viñas, J. Am. Chem. Soc., 2012, 134, 212.
E. Oleshkevich, A. Rosell, A. Morancho, K. Galenkamp, J. Comella F. Teixidor, C. Viñas, Nanomedicine: NBM, 2019, 20, 101986.
The core of the NPs were observed inside
the cells by HR-TEM and CryoTEM.

## Slide 20
PROPOSALS
PROPOSALS at the MIRAS Beamline Fourier Transform Infrared (FTIR) spectroscopy and microscopy.
Boron clusters possess B-H bonds that appear in a peculiar region of the IR spectra in which no other bonds related to organic molecules appear.
- IR spectroscopy can support the presence of multifuctional Boron-containing agents inside cells for their use in multifuctional therapy (BNCT + thermotherapy + chemotherapy): decrease of the secondary effects while maintaining the efficiency.
- Presence of Boron clusters in biopolymers (DNA, gens, bone cements, ….) and polimers (COPs: Polypyrrole, PEDOT,….) …

## Slide 21
New opportunities of boron clusters
in materials and medicine

## Slide 22
Acknowledgements
Prof. Francesc Teixidor
Dr. Elena Oleshkevich
Ms. Isabel Fuentes
Notes: Thanks to all the group in Bellaterra but specially to Elena Oleshkevich, Ms. Isabel Fuentes and Francesc Teixidor.

## Slide 23
COSAN: on the road to anticancer therapies
PROPOSALS at the MIRAS Beamline Fourier Transform Infrared (FTIR) spectroscopy and microscopy.
On Metallacarboranes (CoSAN and FeSAN):
After cellular uptake, would it be possible to discern by
Fourier Transform Infrared spectroscopy and microscopy on
the interaction between:
Metallacarbone and lipids?
Metallacarborane and proteins?
Metallacarborane and DNA?
If interaction was proven, would it be possible to quantify the amount of metallacarborane into the cell? Nucleus?
Notes: If COSAN accumulates within the nucleous, Does COSAN interact with DNS?

## Slide 24
CARBORANES: on the road to anticancer therapies
PROPOSAL at the MIRAS Beamline Fourier Transform Infrared (FTIR) spectroscopy and microscopy.
2) On Carboranes:
After cellular uptake, would it be possible to prove by FTIR that the carborane units at the NPs shell remains bonded to the core of the nanoparticles, either gold or magnetic ones?