## Slide 1
FTIR for polymers
and in-situ experiments
by Martin Kreuzer
- MIRAS-

## Slide 2
The Experiment
*2019 L.S.Dilkes-Hoffman, S.Pratt, P.A.Lant and B.Laycock - The Role of Biodegradable Plastic in Solving Plastic Solid Waste Accumulation
Objective
Stretching stage
Stretching stage
Polymer film
Objective
Polarizer
Setup:
Infrared microspectroscopy

## Slide 3
The Experiment
*2019 L.S.Dilkes-Hoffman, S.Pratt, P.A.Lant and B.Laycock - The Role of Biodegradable Plastic in Solving Plastic Solid Waste Accumulation
Objective
Stretching stage
Stretching stage
Polymer film
Objective
Polarizer
Setup:
Infrared microspectroscopy
Poly lactic acid (PLA)
Polyethylene (PE)
Bioderived
and biodegradable
High brittleness
Material: Polymer blend films
Fossil based and non-biodegradable
Well-known commodity polymer
Excellent mechanical properties

## Slide 4
100 µm
fractured
not-fractured
fractured
not-fractured
100 µm
The Results

## Slide 5
100 µm
fractured
not-fractured
C=O
756 cm-1
CH2
719 cm-1
fractured
not-fractured
100 µm
C=O
756 cm-1
CH2
719 cm-1
The Results

## Slide 6
Mapping and principal component analysis (PCA)
Average spectra
(polarized light)
The Results
Lines

## Slide 7
Mapping and principal component analysis (PCA)
Average spectra
(polarized light)
PCA – Scores plot
The Results
Lines

## Slide 8
Optimum sample characteristics:
Infrared transparent sample (holder) for transmission measurements
Sample thickness between 0.2 and 20.0 µm
Change of orientation by a tuneable parameter (e.g. tensile force, temperature, voltage, light, humidity, …)
Results:
Maps with 5 µm spatial resolution
Measurement time per spectra is around 10 seconds
Martin Kreuzer - MIRAS