## Slide 1
24/02/2020
Workshop ICMAB-ALBA 2020
Carmen Ocal
Towards an in-situ and in real-time view of interfaces
involving small molecules

## Slide 2
MAT2016-77852-C2-1-R (AEI/FEDER, UE)
EU Horizon 2020 under the Marie Skłodowska-Curie Grant agreement No 722651.
Agreement ICMAB-ALBA since 2011
PCSI Group members:
PhD students: Rogger Palacios, Adara Babuji and Francesco Silvestri
Permanent staff: Esther Barrena and Carmen Ocal
ICMAB Research Unit
Functional Surfaces and Interfaces
- Functional Nanomaterials and Surfaces (NANOSURF)
Physical Chemistry of Surfaces and Interfaces (PCSI)
https://departments.icmab.es/surfaces/

## Slide 3
Rivnay et al. Chem. Rev. 2012, 112, 5488
Microstructure and morphology in organic materials for electronic devices
Photovoltaics
Thin Film Transistors
two-component blend film of bulk heterojunctions in organics photovoltaics (OPV)
single component small-molecule semiconductor film used in OFETs
Notes: Size scales and relevant morphological features in organic electronic devices.

## Slide 4
Organic/electrode
Liu et al. Materials Today 2015
Interfaces in a device Organic Field Effect Transistors (OFETs)
Organic/Dielectric
Aghamohammadi et al
ACS Appl. Mater. Interf.2015
Structure & Stability (vs t, T, envir.)
critical issues for properties and performance
Structure determination
Structural/morphological stability over time
Stability of the electronic performance in environmental conditions (O2 , H2O …)
source
drain
Organic semiconductor
gate
dielectric
metal
VSD
- - - - - - - - - - -
VG
Organic/organic
- donor/acceptor (orientation)
- dopant/organic semiconductor (OSC)
(polarization, charge transfer …)
Verlaak et al. Adv. Mat. 2009

## Slide 5: PSCI group Equipment
Atomic force microscopes (AFMs)
(ambient and RH conditions)
-Nanoscale mechanical, electrical, frictional, morphology….
-Properties during device operation (OFETs)
OBME (vapor) and Layer Injection (liquids) in UHV
Growth of ultra thin films
of organic molecules
Located at ALBA
Scanning tunneling microscopy/FM-atomic force microscopy
(STM/FM-AFM in UHV 10-10)
Atomic structure and local
electronic density of states
Agreement ICMAB-ALBA since 2011
Always aware of other needs for deep insight…

## Slide 6: In-situ and/or in real-time studies of organic material
- Evolution of the structure during material deposition under UHV: growth/crystallization
- Phase transformations during annealing/cooling
- Stability/reactivity during interaction with gases: Structural/electronic/compositional changes (oxidation, corrosion, catalysis…)
XRD, XPS, UPS, NEXAFS, XPEEM….with short-time acquisition time: Synchrotron radiation needed
SR-Facilities employed by our group
Elettra (Italy) ESRF (France) Soleil (France) BESSY II (Germany) ALBA (Spain)

## Slide 7
Two examples of interfaces for which we employ SR to investigate molecular doping:
Dopant/organic semiconductor (OSC) ultra-thin-films: charge transfer
Dopant/metal interaction: surface mediated reactions and on-surface chemistry
Synergies and common interests & ideas & plans with NCD-SWEET (E. Solano, M. Malfois)

## Slide 8
Molecular doping in OSCs
Bulk mixture of the OSC and dopant
Jacobs et al. Adv. Mat 2017
Some issues:
Varying doping efficiency
Adverse effect for crystalline order of OSC film
Dopants
Improved properties by interface engineering:
doping with control of structure and nano-morphology
C60F48
Surface charge transfer doping
Improved injection by reduction of the contact resistance
Si
Au
OSC
Ante et al. Small 2011
SiO2
Dopant
Pérez-Rodríguez et al.
ACS Appl. Mater. Int. 2018
Li et al. ACS Appl. Mat.Int. 2015
Diffusion
Mendez et al Ang. Chem. Int. Ed. 2013
Intercalation
Some issues:
Contact doping
C8-BTBT:PS

## Slide 9: AFM-KPFM
(a)
(b)
SiOx
SiOx
SiOx
EF
Evac
3.4 eV
0.2 eV
0.9 eV
0.4 eV
1.3 eV
HOMO
(c)
HOMO shift of Pentacene and increased work function: proof of charge transfer between PEN and C60F48
Cut-off and Valence Band (UPS)
- C60F48 growth depends on the underlying PEN layer and crystallinity.
- C60F48 provokes local variations of work function ()
1L
2L
-1.1 V -0.2 V
Surface potential (KPFM)
Topography
+ 14 Å C60F48
1.5 ML of PEN
on native SiO2
1. Organic/organic interface
1L
2L
C60F48 grows amorphous or crystalline?

## Slide 10: In-situ Structural Investigation
ID03
Linus Pithan
Si
Si
p-type dopant
C60F48
OSC: pentacene
Native SiO2 on Si(001)
XRR
Out of plane
δ
GIXD
In plane
Reciprocal space 2D map
UHV chamber
X-rays
Effusion cell

## Slide 11
(11)
(02)
(12)
(21)
(20)
Silicon
Silicon
Pentacene
Crystalline (111)-oriented fcc C60F48
The underlying Pentacene structure is preserved
Is it possible to “see” where the C60F48 locates?
C60F48 on Pentacene
Silicon
XRD 2D maps

## Slide 12
0 V
1.2 V
AFM
KPFM
NEXAFS PEEM @ F 1s
LEEM FoV= 15µm, E=2.5eV
BESSY II
UE49_PGM SMART
Thomas Schmidt
Fritz-Haber-MPI
XPEEM/LEEM
Space distribution of the dopant?
*Element specific: C60 F48 signature
*Optimized experiments to reduce damage
F K-edge

## Slide 13
Metal (contact)
Au(111)
Ni(111)
Cu(111)
Tsub= RT
STM (Scanning Tunneling Microscopy)
+
FM-AFM (Frequency Modulation Atomic Force Microscopy)
source
drain
Organic semiconductor
gate
dielectric
metal
VSD
- - - - - - - - - - -
VG
Contact doping
2. Organic/metal interface
Beneficial and detrimental effects
C60F48 (dopant)

## Slide 14: C60F48 on Au(111) STM @RT C60F48 on Cu(111)
[11]
[11]
Ordered hexagonal lattice
Inhomogeneous DOS
Ordered hexagonal lattice
Round and 3-lobed DOS
It looks as C60 !!??
@ 8K
Néel et al. Phy. Rev. Lett. 2007
Motai J.Jap.Appl.Phys. 1993
C60 on Cu(111)

## Slide 15: In-situ chemical analysis by XPS
C1s
F1s
C60F48 integrity on Au(111)
C60F48 on Cu(111)
defluorinates and
converts into C60 !!
ICN2_XPS facility (G.Sauthier)
F ̶ C
C ̶ F
C ̶ CF
C60F48 on Cu(111)
C1s
CF
CC
CCF
0.4 ML
0 ML
2 ML
FCu
FC
Auger tail
F1s
F1s
No F
C60F48 on Au(111)
CF
CC
CCF
0.4 ML
0 ML
2 ML
FCu
FC
Auger tail
F1s
C1s
C60F48 is preserved for fully covered Cu(111)
Metal-fluoride forms

## Slide 16
As in Cu(111), the C60F48 dopant defluorinates in Ag(111) and Ni(111)
Chemical stability explored in-situ by NEXAFs/XPS
Elettra @Aloisa
Luca Floriano
Effect of annealing
C60F48
C60
clear difference in electronic orbitals
C60F48 over Ni(111)
J.Faraudo
D.Malaspina
Teo & Simulation @ICMAB
Molecular Dynamics (MD) using reactive Force Field (ReaxFF)
In ReaxFF covalent bond creation/breaking and e- transfer are included explicitly. Temperature control is included

## Slide 17
Near-Ambient Pressure Photoemission (NAPP endstation)
BOREAS: soft X-ray (magnetic) circular and linear dichroism (XMCD/XMLD) measurements
PCSI-ALBA synergies
Sample transfer in UHV
Suitcase ALBA
M. Malfois, E. Solano
Growth facilities @ PCSI

## Slide 18
Atomic Layer Injection (ALI) system_Bihur Crystal
Single molecule solutions
Two or multicomponent solutions
Sequential deposition
Pulse number, pulse duration
Solvent type, concentrations
Substrate temperature
Deposition of non-volatile materials in UHV

## Slide 19
Deposition from vapor phase (sublimation) in UHV for in-situ/real-time GIXD studies
X-rays
Specific designs for NCD-SWEET beamline (ALBA)
UHV chamber
-Deposition time
-Temperature sweep
-Exposure to water or gases
Deposition from liquid solutions in UHV for in-situ/real-time GIXD studies
X-rays
Expands the catalog to non-volatile materials
Permits sequential deposition as well as co-deposition
Opens the way to on-surface synthesis of functional (engineered pores) 2D covalent organic frameworks (COFs)
Allows exploring new combined strategies (vapor + liquid)
Structural phase transitions
Structural changes arising from interaction with gases
Catalysis, gas storage…

## Slide 20
MAT2016-77852-C2-1-R (AEI/FEDER, UE)
EU Horizon 2020 under the Marie Skłodowska-Curie Grant agreement No 722651.
Agreement ICMAB-ALBA since 2011
Rogger Palacios, Adara Babuji and Francesco Silvestri
Esther Barrena and Carmen Ocal
Physical Chemistry of Surfaces and Interfaces (PCSI)
https://departments.icmab.es/surfaces/
Thanks !

## Slide 22
The role of interface dipoles
Metal-organic interface
Covalent
bond
Permanent dipole
Pillow effect
Charge transfer
Cation formation
Anion formation
Ishii et al. Adv. Mater. 1999, 11, 605–625
Push-back effect
Anode
donor
acceptor
cathode
-
+
Organic-organic interface
Organic-organic: polarization, charge reorganization, charge transfer …
The influence of the molecular dipole orientation on the structural and electronic properties of an organic-organic interface remains poorly understood

## Slide 23
Specular intensity XRD for (a) C8-BTBT-C8 film (48nm) and (b) BTBT-C8 film (22nm) before (black line) and after (blue line) a multilayer deposition of C60F48 on top (15nm). The spike at qz=7.8 nm-1 is not a structural feature from the samples.
XRD specular reflectivity of (a) BTBT-C8 (22 nm) and (b) C60F48(15nm)/ BTBT-C8 (22nm). The black curves correspond to the diffraction data acquired at room temperature and the blue curves correspond to the data measured at 80oC for BTBT-C8 and 100oC for C60F48/C8-BTBT-C8.
Topography and (b) simultaneously measured KPFM surface potential (SP) map for C60F48 (2 nm)/C8-BTBT-C8(9nm) on a 200nm thick SiO2. Line profiles along the segments in the (c) surface potential map and (d) topography show the correlation between the increase (decrease) in work function (SP) and the C60F48 crystallites.

## Slide 26
FNi
CC
0,3 ML
0,7 ML
Ni(111)
C1s
F1s
10% of F
40% of F
F at the surface
Full defluorination of the molecules on Ni(111)
C60F48 on Ni(111) XPS