## Slide 1: BL04 MSPD
Materials Science and Powder Diffraction
Aleksandr Missiul
Experiments Division CELLS – ALBA
Carrer de la Llum 2-26, 08290, Cerdanyola del Vallès, Barcelona, Spain

## Slide 2: What is powder diffraction?
2
Peak position 2θhkl
Bragg law :
λ=2*dhkl*sinθhkl
information on overall periodical arrangement of atoms
Peak intensity Ihkl
Structure factor:
type of atom (fj) in material
positions (xj,yj,zj) of atoms in the structure (unit cell)
Peak FWHMhkl
microstructural features (strain, size, stacking faults, …)
Incident beam
Sample
Diffracted beam
2θhkl
0D detector
1D detector
2D detector

## Slide 3: MSPD beamline

## Slide 4: Powder Diffraction Station
Sample Environment:
l-He Dynaflow Cryostat: 5K- RT
700 series lN2 Cryostream 80 – 450 K
FMB Oxford/Cyberstar Hot air blower: RT- 980°C
Capillary flow cell: 80 – 1173K, 0 – 50 bar or 1 – 5 ml/min gas flow
Potentiostat for the electrochemical studies

## Slide 5: Powder Diffraction Station
Propane sorption by ZIF-8
Pump-probe measurements:
polarization/depolarization of PZT

## Slide 6: HP/MD Station
High Pressure:
lHe Cryostat: 15K-RT
External heating air-system: RT- 600 K
External heating vacuum system : RT- 900 K
External heating vacuum system : RT- 1300 K

## Slide 7: HP/MD Station: HP measurements
Journey to the center of Earth
Pressure makes cooling devices
Catalin Popescu Beamline Scientist Tel.: (+34) 93 592 4421 E-mail: cpopescu@cells.es

## Slide 8: Q&A
Thank you for attention!

## Slide 9: Description of the beamline
9

## Slide 10: Powder Diffraction Station
NaCaAlF3, 20keV, Ø0.5 mm
YNiO3
90.0754 º monoclinic distortion
MultiAnalyzerDetector (10 – 50 keV)
13 channels with 1.5 deg pitch
Si111 or Si220 Bragg reflection
YAP scintillator + PMT
Mirror collimating : beam size 3 x 1.5 mm
Full pattern acquisition : 10 min – 2 hours
Scanning speed : (0.5-1°/min)
-> 0.005° angular resolution
Mythen detector (8 – 30 keV)
Si position sensitive detector
6 modules (1280 channels, 50 μm pitch)
ms time resolution
Mirror focusing: beam size 3 x 0.7 mm
Full pattern acquisition :
  ~ms: 1 position / trigger mode (stroboscopic)
  1-5 sec: 1 position, ~40° range
  1 – 10 min: 5 positions , ~60° range
  ~30min: 20 positions, ~130° range (PDF)
-> ~40° in 0.005 deg pitch -> 0.02° angular resolution

## Slide 11: HP/MD Station
HP-MD station (20–50 keV)
2D Rayonix CCD detector ø162 mm
Lorentzian shape focus spot 15x15 μm
150-500 mm sample-detector distance -> 0.05-0.08° angular resolution