## Slide 1
BOREAS for Multiferroics and +
Javier Herrero-Martín. BL29-BOREAS
General sample preparation/form Sintered pellets of policrystalline powder, single crystals (larger than ~100*100 um2), NPs(*), thin films, in-situ metals/molecules deposited onto substrates…
MFs - what can we learn? Chemically-selective quantitative details of the VB electronic structure, local symmetry and magnetization (orbital and spin separately) (HECTOR); CM/ICM AFM order analysis: element-selective magnetic moments orientation (MaRes)
ME coupling - what can we do? i) SHs ready to apply V-bias (or current)  magnetic response via XMLD-XMCD or ii) apply magnetic field in any direction (< 2 T or < 6 T)  electric response via XLD (HECTOR)
Polycrystalline powder - MF like CMTO
Single crystal - Single-phase ME MF like MnCoWO4
Heterostructure - Composite ME MF system like PE STO + magnetostrictive substrate
Three examples
Special thanks to: J.L.García (ICMAB-CSIC), L. Maurel (ETH-PSI), J. Ruiz-Fuertes (UNICAN), G. Subías (ICMA-UZ)

## Slide 2
Td
0.50
xy, xz, yz
xz, yz
xy
0.15
3z2-r2
0.30
x2-y2
0.20
xz, yz
3z2-r2
0.36
xy
0.09
x2-y2
0.50
xz, yz
3z2-r2
0.40
xy
1.30
x2-y2
1.00
x2-y2, 3z2-r2
D4h elong.
C4h S.D.
C4h L.D.
Calculated XAS
Calculated XMCD
Mn L2,3
X-ray absorption (arb. units)
5 K, 6 T
1. Polycrystalline powder - MF like CaMnTi2O6
Mn2 sites in D4h symmetry, not square planar (contrarily to as claimed) (E3z2-r2 > Exy)
Mn1 & Mn2 moments add up parallel in the AFM phase
PRB 97, 235129 (2018)

## Slide 3
2. Heterostructure - Composite ME MF like PE STO + magnetostrictive substrate
in preparation (2020)
mS=0.018, mL=-0.013  mTOT=0.004
X-ray absorption (arb. units)
(a)
(b)
Experimental, 5 K
Calculated
Ti L2,3
*30
*30
(CMTO)
B-field applied, electric response via charge redistribution seen in XLD

## Slide 4
orbital, spin
χ
η
3. Single crystal - Single-phase ME MF like MnCoWO4
PRB 91, 220403(R) (2015)
Element-selective (Mn, Co) magnetic structure unveiled thanks to RMXS
actual AFM structure
RMXS to complement Neutron Diffraction
As seen by ND
Small samples
High momentum space resolution (ICM structures)
Orbital / spin separation (non-res.)
More than one magnetic element (resonant)
unrotated
sum
rotated
calculated:
experimental
Calc. sum

## Slide 5
1
2
ME coupling is due to Mn spins as demonstrated by RMXS
V
~ 102-103 V
c
b
3. Single crystal - Single-phase ME MF like MnCoWO4